Supplementary Material

High tribo-corrosion resistance of Ni-Cr-5Al2O3 thermal spray coating: a comparison of post processing techniques

Mayank Gar et al.

DOI 10.1515/corrrev-2024-0065

Supplementary Figure S1: BSE image river sand.

Supplementary Figure S2: Electrical equivalent circuit (EEC) diagram for fitting of impedance spectra.

Supplementary Table S1: Chemical composition of SS316L.

| Element | C | Si | Mn | P | S | Cr | Ni | Mo | N |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Weight % | 0.09 | 0.28 | 0.92 | 0.01 | 0.01 | 18.82 | 9.89 | 1.93 | 0.00 |

Supplementary Table S2: Test parameters used for the slurry erosion testing.

| Parameters | Value |
| --- | --- |
| Stand-off distance | 20 mm |
| Sand particle concentration | 5000 ppm |
| Sand particle size | 75-150 µm |
| Angle of impact | 30°, 90° |
| Jet velocity | 20 m/s |
| Test duration | 2 h |