SUPPLEMENTARY DATA

Table S1. Number of replicates used for each voltage and corresponding power density. 

	Voltage

(V)
	Power density

(W/cm2)
	 Replicates

 F-P105
	Replicates P105

	90
	1.009
	3
	----

	95
	1.062
	9
	----

	100
	1.030
	9
	6

	105
	1.267
	9
	6

	110
	2.183
	9
	6

	115
	2.389
	9
	6

	120
	2.546
	6
	6

	125
	3.540
	4
	6

	130
	5.013
	9
	6

	135
	5.432
	14
	6

	140
	5.914
	12
	6


Table S2. Alpha, beta and lambda values (for folated and non-folated micelles). Values are averages of the replicates shown in Table S.1.

	
	[image: image1.png]


 (µm-1.s-1)
	[image: image2.png]


 (µm3/s)
	λ (µm/s)

	Power density (W/cm2)
	F-P105
	P105
	F-P105
	P105
	F-P105
	P105

	1.009
	0.006003
	---
	211.4
	---
	258.6
	---

	1.062
	0.007998
	---
	522.4
	---
	296.9
	---

	1.030
	0.01087
	0.01713
	576.7
	901.9
	355.6
	675.8

	1.267
	0.01118
	0.01510
	653.9
	772.7
	232.2
	418.7

	2.183
	0.02151
	0.01869
	431.6
	1243
	351.3
	345.1

	2.389
	0.02230
	0.02523
	837.2
	1916
	288.6
	317.2

	2.546
	0.03199
	0.02655
	2052
	2491
	302.5
	319.2

	3.540
	0.03972
	0.04016
	2171
	2003
	414.1
	488.8

	5.013
	0.05905
	0.05016
	2620
	3116
	697.1
	611.4

	5.432
	0.05741
	0.04912
	3601
	3360
	529.0
	506.0

	5.914
	0.04851
	0.02995
	3098
	2225
	382.6
	329.0


