# SUPPLEMENTARY MATERIAL

Table S.1. Final release percentages obtained using 20-kHz, 1-MHz and 3-MHz US at the indicated power densities. The final release at 20 kHz was obtained after 10 min of insonation, while at 1 and 3 MHz was obtained after 60 min.

| pH | Frequency | Liposomes | Power density (W/cm2) | Percentage release |
| --- | --- | --- | --- | --- |
| 5.2 | 20 kHz | non-PEGylated | 6.08 6.97 11.83 17.14 | 74.53±7.56 74.64±4.73 74.50±2.48 87.21±5.36 |
|  |  | PEGylated | 6.08 6.97 11.83 17.14 | 71.48±15.09 75.96±9.49 81.81±7.87 88.30±5.82 |
| 7.4 | 20 kHz | non-PEGylated | 6.08 6.97 11.83 17.14 | 86.44±7.43 94.52±8.69 93.20±6.26 97.14±6.76 |
|  | 20 kHz | PEGylated | 6.08 6.97 11.83 17.14 | 70.76±8.47 77.19±2.17 83.57±6.03 94.91±6.16 |
|  | 1 MHz | PEGylated | 10.5 18.7 27.6 39.2 50.2 | 4.18±0.15 14.87±0.09 41.34±1.21 48.43±0.49 55.43±1.66 |
|  | 3 MHz | PEGylated | 50.6 78.5 94.3 158.5 173.3 183 | 4.32±0.16 31.34±2.76 32.71±1.13 60.61±0.91 60.74±0.79 67.04±1.63 |