Ultra-compact On-Chip Photo-thermal Power Monitor based on Silicon Hybrid Plasmonic Waveguides

Hao Wu1,2, Ke Ma1,2, Yaocheng Shi1,2, Lech Wosinski2,3, and Daoxin Dai1,2,*

1. Centre for Optical and Electromagnetic Research, State Key Laboratory for Modern Optical Instrumentation, Zhejiang Provincial Key Laboratory for Sensing Technologies, Zhejiang University, Hangzhou 310058, China;
2. JORCEP, Joint Research Center of Photonics of the Royal Institute of Technology (Sweden) and Zhejiang University, China;
3. School of Information and Communication Technology, KTH Royal institute of Technology, 164 40, Kista, Sweden.

*Corresponding Author: dxdai@zju.edu.cn

1. The simulated temperature distribution T(x, y, z).

Fig. S1A shows the simulated temperature profiles T(x0, y0, z) in the metal strip when choosing lm = 2, 3, 5, 10, and 20 μm, respectively. Here x0 = 0, and y0 = 0. The two insets show the simulated temperature distribution T(x, y0, z) at the top surface of structure when lm = 2, and 20 μm, respectively. It is obvious that optical power decreases exponentially when light propagates along the HPWG. As a result, the absorbed power of light decreases exponentially, and thus the temperature in the metal strips is non-uniform distribution along the propagation direction z. Fig. S1A shows that there is a maximal temperature variation at around z = 0.8 μm, instead of z = 0 (i.e., the front end of the metal strip). The reason is that there is some heat dissipation from the metal strip to the silicon core connected at the front end. One also observes that the temperature increases as the length lm increases from 2 μm to 5 μm because more optical power is absorbed and less heat dissipation from the metal strip to the silicon core connected at the back end. When lm > 5 μm, almost 100% of optical power is absorbed and no heat dissipates from the metal strip to the silicon core connected at the back end. Thus the temperature profile T(x0, y0, z) becomes insensitive to the length lm, as shown in Fig. S1A.

Fig. S1B shows the temperature profile T(x, y, z0) at the cross section of HPWG when 1mW optical power is applied. The inset curve shows the temperature distribution T(x0, y, z0) along the y direction in the middle of HPWG. It is shown that the temperature in the metal strip and silicon core is uniform due to the high thermal conductivity of platinum (71.6 Wm-1K-1) and silicon (149 Wm-1K-1). The temperate decreases in the SiO2 layer because of the low thermal conductivity (1.4 Wm-1K-1), which helps to preserve heat dissipation.

- (A) The temperature distribution T(x0, y0, z) in the metal strip on HPWGs when lm = 2, 3, 5, 10, and 20 μm, respectively. The inserts show the calculated temperature distributions T(x, y0, z) when lm = 2 μm and 20 μm. (B) The cross-sectional temperature profile T(x, y, z0) and the temperature profile T(x0, y, z0). Here x0=0, y0=0, z0=0, and Pin = 1 mW. The parameters are given as follows: wm = 400 nm, hsi = 225 nm, hSiO2 = 50 nm and hm = 80 nm.

2. Calculation of the average temperature variation  in the metal strip.

Since the metal strip is heated non-uniformly, as shown in Fig. S1A, its resistivity also becomes non-uniform along the z direction. In order to evaluate the responsivity conveniently, here we define an average temperature variation  to describe the temperature variation in the metal strip.

Regarding that the cross-sectional temperature distribution of the metal strip is uniform, the temperature in the metal strip can be simply described as T = T(z), 0 ≤ z ≤ lm. Accordingly, the resistivity along the propagation direction z is given as

,

where T0 is the initial temperature (usually room temperature) when the input optical power Pin = 0, ρ0 is the resistivity at T = T0, α is the temperature coefficient of resistivity (TCR). The resistance of the metal strip is then given by the following integration form

,

where wm, hm and lm are the width, the thickness and the length of the metal strip, respectively. By substituting Eq.  into Eq. , one has

,

i.e.,

.

Eq.  is then rewritten as

,

where R0 is the resistance when Pin = 0, and one has

.

By defining the average temperature variation  as

,

from Eq.  one has

.

3. Dependence of the performances on the SiO2 thickness hSiO2.

Apparently the sizes of the HPWGs have an impact on the performance (e.g. responsivity and dynamic range) of the power monitor. Here the dependence of the responsivity on the thickness hSiO2 of the SiO2 layer between the metal strip and the silicon core region is analyzed numerically. As an example, we choose the length of the metal strip as lm=15 μm.

Fig. S2A-B show how the SiO2 thickness hSiO2 influences the absorption coefficient αabs of an HPWG, the average temperature variation , and the highest temperature Tmax in the metal strip, respectively. From Fig. S2A, it can be seen that the metal absorption coefficient αabs decreases as the thickness hSiO2 increases (because less electric field penetrates into the metal layer [S1]). Therefore, it is expected to see that the average temperature variation  decreases as the thickness hSiO2 increases. On the other hand, as SiO2 has much smaller thermal conductivity (1.4 Wm-1K-1) than silicon (149 Wm-1K-1), the increase of the SiO2 thickness helps to preserve heat dissipation from the metal strip to the silicon core and the substrate. As a consequence, the average temperature variation  becomes higher. Therefore, there is an optimal SiO2 thickness (e.g., hSiO2 = ~0.26 μm here) for maximizing the average temperature variation  when the SiO2 thickness increases from 0.02 μm to 1 μm, as shown in Fig. S2B.

From Fig. S2B, it can be seen that the highest temperature Tmax increases greatly as the thickness hSiO2 decreases from 1.0 μm, which is due to the stronger absorption. However, when the thickness hSiO2 is reduced further to be very small (e.g., <0.15 μm), the HPWG becomes very lossy with very high absorption coefficient (e.g., ~6 dB/μm when hSiO2 = 20 nm) and heat is generated mostly at the front end of the metal strip. Thus more heat is dissipated to the silicon nanowire connected at the front end, which leads to a slight reduction of the maximal temperature Tmax. From Fig. S2B, one can choose relatively large thickness hSiO2 to achieve a reduced maximal temperature Tmax so that higher upper-limit for the input optical power can be achieved.

In our case, as we chose a silicon-on-insulator (SOI) wafer with a 250nm-thick top-silicon layer and the SiO2 layer was formed by oxidizing the top silicon layer at a high temperature. Since the top silicon layer should be thick enough for waveguiding, we choose the SiO2 thickness as hSiO2 = 50 nm (in which case the thickness of the top silicon is about 225 nm). As indicated by Fig. S2B, it is possible to improve the performance (e.g., responsivity and dynamic range) by making the SiO2 layer as thick as 260 nm with the plasma enhanced chemical vapour deposition (PECVD) technique.

- (A) The absorption coefficient αabs as the SiO2 thickness increases; Inset: the mode profiles when hSiO2 = 0.02, 0.1 and 0.5 μm, respectively. (B) The calculated average temperature variation  and the highest temperature Tmax in the metal strip as the SiO2 thickness hSiO2 increases; Here wm = 400 nm, hSi = 225 nm, hm = 80 nm, lm = 15 μm, and Pin=1 mW.

4. Dependence of the performances on the thickness hm of the metal strip.

Fig. S3A shows the dependence of the absorption of HPWG on the thickness hm of the metal strip. It can be seen that the absorption coefficient αabs is not sensitive to the thickness hm when hm > 0.1 μm. The average temperature variation  and the highest temperature Tmax decreases as the thickness hm increases from 0.1μm (see Fig. S3B). This is because of the increase of the heating volume of metal.

In contrast, when hm < 0.1 μm, the absorption increases significantly as the thickness hm decreases, as shown in Fig. S3A. This is because the surface plasmon enhancement also occurs at the top-surface of the metal layer when the metal layer is ultra-thin (see in insets of Fig. S3A). In this case, most of the input optical power is absorbed within very short propagation distance starting from the frond-end of the metal strip. Due to the very high absorption, heat is most localized at the front-end of the metal strip, which leads to a strong heat dissipation from the metal strip to the SOI nanowire connected at the front end. Therefore, there is an optimal thickness for the metal layer to maximize the average temperature variation . In our design, we choose hm = ~0.08 μm, where the average temperature variation  becomes maximal.

- (A) The absorption coefficient αabs as the metal thickness hm increases; (B) The calculated average temperature variation  and the calculated highest temperature Tmax in the metal strip as the metal thickness hm increases from 0.02 μm to 1 μm. Here wm = 400 nm, hSi = 225 nm, hSiO2 = 50 nm, lm = 15 μm, and Pin = 1 mW.

Reference

- Dai D, He S. A silicon-based hybrid plasmonic waveguide with a metal cap for a nano-scale light confinement. Opt. Express 2009; 17(19): 16646–16653.