Supporting information: Origin of dispersive line shapes in plasmon-enhanced stimulated Raman scattering microscopy

Cheng Zong1, Ji-Xin Cheng1,2*

1. Department of Electrical and Computer Engineering, Boston University, Boston, Massachusetts 02215, USA.

2. Department of Biomedical Engineering, Photonics Center, Boston University, Boston, Massachusetts, 02215, USA.

*Corresponding author: email: jxcheng@bu.edu

SI1. The resonant and nonresonant nonlinear susceptibility in the spectral domain.

Figure S1. The stimulated resonant and nonresonant nonlinear susceptibility in the spectral domain. The real part (black) and imaginary part (red) of resonant susceptibility (). The nonresonant part (): blue. The half width at half maximum of Raman line is 5 cm-1. Here, we note that  is a Lorentzian line shape and  can be rewritten as a Fano-line shape in which the Fano parameter is 1 as following:

(S1)

SI2 Delay time traces obtained from Au NPs substrate with/without adenine adsorption

Figure S2. Delay time traces obtained from the adenine adsorbed Au NPs substrate and the Au NPs substrate without adenine adsorption.

SI3 SRL and SRG spectra and images of solid adenine

Figure S3 a) The SRL and SRG images of adenine. b) The SRL and SRG spectra of adenine.

SI4. Fano-like fitting results of PESRS spectra from adenine adsorbed on Au NPs

Table S1 Results from the Fano-like fitting of the PESRL and PESRG data from adenine

|  | x0 (cm-1) | (cm-1) | A |
| --- | --- | --- | --- |
|  | 732.9 | 10.3 | 0.059 |
| PESRL | 732.6 | 9.6 | 0.0732 |
|  | 732.2 | 9.3 | 0.0615 |
|  | 733.0 | 10.3 | 0.0102 |
| PESRG | 733.1 | 9.7 | 0.0143 |
|  | 732.8 | 10.9 | 0.0105 |

The fitting function is shown as following: fx=A(q+x-x0/2)21+(x-x0/2)2-(x-x0/2)21+(x-x0/2)2. Here, A is the amplitude of the peak, x0 is the center frequency of vibrational feature,  is the line width. q is the Fano asymmetry parameter. The q= 1.7 and q = 2 are used to fit the PESRL and PESRG data, respectively.