Supplemental materials for

# A high-gain cladded waveguide amplifier on erbium doped thin-film lithium niobate fabricated using photolithography assisted chemo-mechanical etching

Youting Liang1, 2, Junxia Zhou1, 2, Zhaoxiang Liu2, Haisu Zhang1, 2, *, Zhiwei Fang2, Yuan Zhou3, Difeng Yin3, Jintian Lin3, Jianping Yu3, Rongbo Wu3, Min Wang2, and Ya Cheng1, 2, 3, 4, 5, 6, *

1State Key Laboratory of Precision Spectroscopy, East China Normal University, Shanghai 200062, China.

2The Extreme Optoelectromechanics Laboratory (XXL), School of Physics and Electronic Sciences, East China Normal University, Shanghai 200241, China.

3State Key Laboratory of High Field Laser Physics and CAS Center for Excellence in Ultra-Intense Laser Science, Shanghai Institute of Optics and Fine Mechanics (SIOM), Chinese Academy of Sciences (CAS), Shanghai 201800, China.

4Shanghai Research Center for Quantum Sciences, Shanghai 201315, China.

5Collaborative Innovation Center of Extreme Optics, Shanxi University, Taiyuan 030006, China. 6Collaborative Innovation Center of Light Manipulations and Applications, Shandong Normal University, Jinan 250358, China.

*Correspondence: Haisu Zhang (hszhang@phy.ecnu.edu.cn), Ya Cheng (ya.cheng@siom.ac.cn).

In the Supplemental materials we describe the waveguide fabrication process by PLACE and the theoretical model for the erbium-doped waveguide amplifier.

The waveguide fabrication process by PLACE

Fig. S1 Schematic illustration of waveguide fabrication process by PLACE.

The waveguide fabrication procedures by PLACE are schematically illustrated in Fig. S1, including (1) deposition of a thin layer of chromium (Cr) with a thickness of 400 nm on the LNOI wafer by magnetron sputtering, and (2) patterning of the Cr film using femtosecond laser ablation, (3) pattern transferring from the Cr mask to the underneath LN thin film by chemo-mechanical polishing (CMP), (4) removal of remaining Cr mask and a secondary CMP. After the waveguide is shaped, a thin layer of Ta2O5 is deposited on top of LNOI by sputtering coating. The smooth sidewalls of the fabricated LNOI waveguides are guaranteed by CMP which can maintain subnanometer surface/interface roughness comparable with the surface-tension induced atomic scale finish.

The theoretical model of Er3+-doped waveguide amplifier

The Er3+-doped amplifier model introduced in Refs. [8, 9] is employed, which includes the steady-state response of the three-level Er3+ with 4I15/2, 4I13/2, and 4I11/2, and the migration-accelerated ETU process and the concentration quenching of erbium ions. The involved transitions are shown in Fig. S2.

Fig. S2 The involved Er3+ energy levels in the amplifier model. (a) the 3-level system for active ions. (b) the migration-accelerated ETU process. (c) the 3-level system for quenched ions. The blue wavy arrows denote fast decay.

The steady-response of Er3+ in the pump and signal fields can be obtained by the equations below:

dN2dt=FPσaPN0-σePN2+WETUN12-1τ2N2=0  							(1)

dN1dt=FsσaSN0-σeSN1+1τ2N2-2WETUN12-1τ1N1=0 					(2)

N0+N1+N2=Nd 														(3)

where Ni(i=0, 1, 2) denote the population density of 4I15/2, 4I13/2, and 4I11/2 states, Nd is the total density of Er3+, τ2 is the non-radiative decay time from 4I11/2 to 4I13/2, τ1 is the intrinsic decay time of 4I13/2, WETU is the macroscopic migration parameter for (4I13/2, 4I13/2)→(4I15/2, 4I9/2), σaP(σaS) and σeP(σeS) are the absorption and emission cross sections for the pump (signal) light. FP=IPhνP and FP=IShνS are the photon fluxes of the pump and signal light, with IP(IP) and νP(νS) being the pump (signal) intensity and frequency. The excited population of the 4I9/2 level by ETU is not included since it will decay to the 4I11/2 level by fast multiphonon relaxation in less than 1 μs.

For the concentration quenching, a small fraction (fq) of Er3+ is assumed to decay rapidly from excited states by static ETU among active ion-pairs or clusters, and excited state trapping by host material defects, resulting in a luminescence lifetime of quenched ions on the order of 1 μs. The response of quenched ions can also be described by equations (1)-(3) with the replacement of the total ion density Nd and the excited level lifetimes τ2&τ1 by fqNd and τq, respectively. The total optical gain is obtained by summing up the steady-state responses of active ions (1-fq)Nd and quenched ions fqNd.

Excited-state absorption (ESA) at the pump wavelength is included as a loss factor in the light propagation along the Er3+-doped waveguide, which written as:

dPPzdz=PPzΨPx,yσePN2-σESAPN2-σaPN0dxdy-α 				(4)

dPSzdz=PSzΨSx,yσeSN1-σaSN0dxdy-α 						(5)

PPz and PSz are the pump and signal powers at the waveguide length z, α is the waveguide passive propagation loss. ΨPx,y and ΨSx,y are the normalized modal field intensities at the pump and signal wavelengths obtained from finite element simulation.

The utilized parameters for Er3+:LNOI waveguide amplifier are listed in table S1.

| Parameter | Value | Source |
| --- | --- | --- |
| σaS | 1.95×10-20 cm2 | [27] |
| σeS | 1.55×10-20 cm2 | [27] |
| σaP | 0.85×10-20 cm2 | [27] |
| σeP | 0 | [27] |
| σESAP | 1.0×10-22 cm2 | [28] |
| WETU | 1.0×10-18 cm3/s | [28] |
| τ2 | 200 μs | [28] |
| τ1 | 2.35 ms | [29] |
| τq | 1 μs | [9] |
| fq | 0, 0.1, 0.2 |  |
| λP | 976 nm |  |
| λS | 1532 nm |  |
| α | 0.1 dB/cm |  |
| Nd | 1.9×1020 cm-3 |  |