Supporting Information

High-Performance Near-Infrared Photodetectors based on Gate-Controlled Graphene–Germanium Schottky Junction with Split Active Junction

Cihyun Kim, Tae Jin Yoo, Min Gyu Kwon, Kyoung Eun Chang, Hyeon Jun Hwang, and Byoung Hun Lee*

- Circular transmission line method

Circular transmission line method (CTLM) test structures were fabricated to determine the quality of the contacts. A CTLM structure comprises of an inner circular contact surrounded by an annular gap within a larger contact area. Each measurement set contained multiple CTLMs with varying gap sizes. The measured total resistance can be expressed as

Rtot=Rsh2πlnL+dL+LTI0L/LTLI0L/LT+LTK0L+d/LTL+dK1L+d/LT,		    (S1)

where I0, I1, K0, and K1 are the modified Bessel functions, LT is the transfer length, L is the radius, and d is the gap spacing. When L>4LT, then I0L/LTI0L/LT and K0L+d/LTK1L+d/LT can be approximated as unity; therefore, Equation S1 simplifies to:

Rtot=Rsh2πd+2LTC,    C=Ldln1+dL,			(S2)

where C is the correction factor.

For each contact-resistivity measurement, the resistances of multiple CTLM structures with different gap spacings d were measured. Rtot is a nonlinear function of d; however, Rtot/C yields a linear function of d with a slope of Rsh/(2π) with d=-2LT when Rtot/C = 0. The sheet resistance and transfer length can then be extracted from a linear fit to Rtot/C.

Figure S1 shows the measured total resistance as a function of the gap spacing and corrected resistance Rtot/C with a linear fit to the corrected data. From the linear fit, the values of LT and Rsh can be extracted, and the contact resistivity ρc can be calculated as

ρc=LT2×Rsh					  (S3)

Figure S1. Resistance values for a CTLM structure with the linear fit are used to calculate the contact resistivity and sheet resistance. In this study, a 45 nm AgSb alloy (Ag with 1% Sb) was formed on the Ge region using a lift-off process, followed by the rapid thermal annealing process for 5 min in a N2 atmosphere at 450 °C.

- Setup for measuring the photocurrent characteristics

A continuous-wave laser beam with a wavelength of 1550 nm from the solid-state laser diode and controller (Thorlabs LPSC-1550-FC and CLD1010LP) was focused onto the sample through a 40× objective lens (Olympus LUCPlanFLN, NA=0.6). The electrical measurements were performed using a Keithley Model 4200 parameter analyzer. The incident light power was 10 W. A Newport Model 1918-C hand-held optical power meter and a 919P-003-10 thermopile sensor were used to measure the optical power. All measurements were performed under ambient conditions (T = 300 K, P = 1 atm) in air.

Figure S2. Diagram of the photocurrent measurement setup.