Supplementary Material for
Ultrafast charge transfer enhanced nonlinear optical properties of CH3NH3PbBr3 perovskite quantum dots grown from graphene

Ye Yuan#, Fenglin Cao#, Peng Li, Jiawen Wu, Baohua Zhu* and Yuzong Gu*
Physics Research Center for Two-Dimensional Optoelectronic Materials and Devices, School of Physics and Electronics, Henan University, Kaifeng 475004, China

[image: image1.png]



Figure S1: The TEM images of (a) PQDs-G1, (b) PQDs-G3. The insets show the size statistics of PQDs grown on G. PQDs in different PQDs-G composite samples have similar distribution and size. The PQDs of PQDs-G1 have an average diameter of 2.3 nm with a size deviation of 0.7 nm, and PQDs of PQDs-G3 have an average diameter of 2.6 nm with a size deviation of 0.8 nm.
[image: image2.png]~
o
—

Intensity (a.u.)

PQDs

45 days

0 day

10

20

30

20 (degree)

40

50

(b)

Intensity (a.u.)

PQDs-G1

10 20 30
20 (degree)

40 50




Figure S2: The time-evolution of the XRD patterns of (a) pure PQDs, (b) PQDs-G1 exposed to the air for 0 day and 45 days. XRD was used to investigate the changes in the crystallinity and phase purity of pure PQDs and PQDs-G composite. The XRD diffraction peak around 12° split into two peaks after PQDs was exposed to the air for 45 days while the XRD diffraction peak of the PQDs-G composite had no obvious change, which indicate the stability was improved by the introduction of G.

[image: image3.png]Absorption (a.u.)

Ut

GO

PQDs-G1
PQDs-G3
PQDs-GS

200

|
300

Wavelength (nm)

400




Figure S3: The UV-Vis absorption spectra of GO and PQDs-G in the range of 200-400 nm. 
