Supporting Information (SI)

Exploring Magneto-Optic Properties of Colloidal Two-Dimensional Copper Doped CdSe Nanoplatelets

Avisek Dutta,1 Amani Saleh Almutairi,2 Jojo P. Joseph,1 Alexander Baev,1 Athos Petrou,2 Hao Zeng,2* and Paras N. Prasad1,2*

1 Department of Chemistry and The Institute for Lasers, Photonics and Biophotonics,

University at Buffalo, SUNY, Buffalo, New York 14260, United States

2Department of Physics,

University at Buffalo, SUNY, Buffalo, New York 14260, United States

Figure S1: (a) TEM images of undoped CdSe NPLs (inset: HRTEM image), (b) the SAED image of undoped CdSe NPLs, and (c) XRD data of undoped CdSe NPLs

Figure S2: AFM images of undoped NPLs (upper) and doped NPLs (lower).

Figure S3: EPR spectra of Copper doped CdSe NPLs

Figure S4: UV – Vis and PL spectra of undoped CdSe NPLs.

Figure S5: Excitation spectra of Copper doped CdSe NPLs at dopant emission wavelength.

Figure S6: Average decay profile of undoped CdSe NPLs measured at band edge area.

Figure S7: Magneto-PL of undoped CdSe NPLs; (a) at 0 T and (b) 7 T at a particular cryogenic temperature (3.7 K).

Figure S8: Circular Polarization as a function of magnetic field (B) at a lower temperature (3.7 K) for the Cu doped CdSe NPLs sample.

Figure S9: Magnetic Field vs Magnetic Moment plot for copper doped CdSe NPLs.