Erik H. Waller, Stefan Duran, Georg von Freymann

Supplementary

Figure S 1: Transmittance spectrum of the final silver solution.

Figure S 1: Transmittance spectrum of the final silver solution.

Transmittance spectrum of photosensitive suspension

Conductivity measurements

Figure S 2: Reflection light microscopy image of a direct laser written beam connecting two electrodes.

Figure S 2: Reflection light microscopy image of a direct laser written beam connecting two electrodes.

To conduct 4-point conductivity measurements first two electrodes were fabricated as follows: a Tollens reagent solution was exposed to UV light until a silver mirror formed. Using a razor blade, the thin silver layer was cut in two halves and electrical disconnection was verified. Between those electrodes a silver beam with 10 x 10 x 50 microns3 was fabricated using direct laser writing as shown in Figure S2. A home-built 4-point measurement device was used to measure the resistance of the thin silver layer alone (0.8 Ω) as well as the silver beam plus the silver layer (15.6 Ω). Using a thin wire model the resistivity was calculated by (Rbeam+layer – Rlayer)*Abeam/lbeam, where Abeam is the area of the cross-section and Ibeam is the length of the beam.