Supplementary information

Switchable Dual-Mode Nanolaser: Mastering Emission and Invisibility through Phase Transition Materials

Sergey Lepeshov1, Andrey Vyshnevyy2, and Alex Krasnok3,4,*

1Department of Electrical and Photonics Engineering, DTU Electro, Technical University of Denmark, Building 343, DK-2800 Kgs. Lyngby, Denmark

2Emerging Technologies Research Center, XPANCEO, Dubai Investment Park 1, Dubai, United Arab Emirates

3Department of Electrical and Computer Engineering, Florida International University, Miami, FL 33174, USA

4Knight Foundation School of Computing and Information Sciences, Florida International University, Miami, FL 33199, USA

*E-mail: akrasnok@fiu.edu

Optical properties of Sb2S3

Sb2S3 is a prospective phase-change material with a high dielectric constant, low loss, and strong tunability in the visible range [1,2]. The permittivity dispersion of Sb2S3 is shown in Figure S1, and it indicates the broadband transparency of this material above the wavelength of 600 nm in the amorphous phase.

Figure S1. – (a) Real and (b) imaginary dielectric permittivity of Sb2S3 in amorphous (blue) and crystalline (red) phases.

Nanolaser model

To find the steady-state charachteristics of the nanolaser we employ a model based on the Keldysh technique for non-equilibrium Green’s functions (NEGF) and the Kadanoff–Baym equations [3]. For convenience, here we brief the main results of the paper and apply them to our nanolaser. From the Kadanoff–Baym equations we derive the spontaneous and stimulated transition rates in the form similar to Fermi’s golden rule integrals:

Rsp≈2πNg2ℏ2n21-n1dωρeωρω,				 (S1)

Rstim≈2πNg2ℏ2n2-n1∫dωρeωSω.				(S2)

where N is the number of emitters, n1 and n2 are the populations of the ground and the excited states of emitters, g is the light-matter coupling constant, ρeω=Γ/(2π)ω-ω02+Γ/22 is the joint density of states of the quantum emitters, ρω is the optical density of states and Sω is the lineshape function which is related to the population of the laser mode as Sωdω=Np.

Equations (S1) and (S2) are fully equivalent to Fermi’s golden rule if we set ρω=κ/(2π)ω-ωMQ2+κ/22 and Sω=Npρω, where ωMQ and κ are the angular frequency and the photon loss rate of the laser (magnetic quadrupole) mode. However, within NEGF framework

ρω=-1πImGRω=-1πIm1ω-ωMQ+iκ/2+ΠintR(ω), 			(S3)

where

ΠintRω=-g2Nn2-n1ω-ω0+iΓ/2,					(S4)

is the contribution of the light-matter interaction with the laser mode to polarization operator. The optical density of states coincides with the common Lorentzian function at transparency (n2=n1) but drastically differs from it when the gain medium is driven close to the lasing threshold. As a result the Purcell enhancement becomes gain-dependent. This effect is significant for “bad cavity” lasers where κ is comparable with Γ.

The balance of photon generation and loss holds not only for the transition rates Rsp+Rstim=κNp but also for their spectral densities

2πNg2ℏ2n2-n1ρeωn21-n1n2-n1ρω+Sω=κSω. 		(S5)

which determines the lineshape function. Set of equations (S1-5) fully determines the steady state of the laser at a given population inversion. Also, they describe effects of frequency pulling, superradiance and yield the threshold population inversion consistent with the semisclassical Maxwell–Bloch model.

Insering the functions ρω determined from Eqs. (S3,4) into Eq. (S1) we find the total spontaneous emission rate

Rsp=14GΓn21-n1n2-n1κ+Γ-G/2 ω0-ωMQ2+κ+Γ-G/222, 			(S6)

where G=κggth1+4ω0-ωMQκ+Γ2 with gth is the threshold material gain. The stimulated ^emission rate is determined as Rstim=κNp-Rsp, where

Np=Sωdω=ΓΓ+κn21-n1n2-n1ggth-g. 			(S7)

Nanolaser coherence

To determine the coherence threshold, we have employed Langevin equation approach. In particular, we have estimated the threshold conditions using the approximate equation (13) of work [4] that can be reformulated in terms of threshold photonic population as Np≈Ngth/(dg/dn2)≈23. However, it is worthy to employ a more accurate equation (9) which reads

g(2)0=1+A2Drr+2ACDsr+AD+BC+C2DssB+CAD+BCNp2 				(S8)

where A, B, C, and D are the coefficients of rate equations linearized close to the stationary point and Dij are the diffusion coefficients that characterize strengths of the Langevin forces.

Figure S2. – Second-order coherence function calculated using Eq. (S8). At threshold g(2)0=1.5 the absorbed pump power reaches about 50 μW which corresponds to 5.6 photons inside the mode.

References:

[1]	S. K. Chamoli, G. Verma, S. C. Singh, and C. Guo, Phase Change Material-Based Nano-Cavity as an Efficient Optical Modulator, Nanotechnology 32, (2021).

[2]	W. Dong, H. Liu, J. K. Behera, L. Lu, R. J. H. Ng, K. V. Sreekanth, X. Zhou, J. K. W. Yang, and R. E. Simpson, Wide Bandgap Phase Change Material Tuned Visible Photonics, Adv. Funct. Mater. 29, 1806181 (2019).

[3]	A. A. Vyshnevyy, Gain-Dependent Purcell Enhancement, Breakdown of Einstein’s Relations, and Superradiance in Nanolasers, Phys. Rev. B 105, 085116 (2022).

[4]	A. A. Vyshnevyy and D. Y. Fedyanin, Lasing Threshold of Thresholdless and Non-Thresholdless Metal-Semiconductor Nanolasers, Opt. Express 26, 33473 (2018).