Supplementary Information

Fine-tuning biexcitons-plasmon coherent states in a single nanocavity

Kun Liang,1 Lei Jin,2 Xuyan Deng,2Ping Jiang,3 and Li Yu*4

1 School of Electronic Engineering, Beijing University of Posts and Telecommunications, 10 Xitucheng Road Beijing, China

2 School of Science, Beijing University of Posts and Telecommunications, 10 Xitucheng Road Beijing, China

3 School of Science Microelectronics and Data Science, Anhui University of Technology, Maanshan, China

4State Key Laboratory of Information Photonics and Optical Communications, School of Science, Beijing University of Posts and Telecommunications, 10 Xitucheng Road, Beijing, 100876, China

*E-mail: yuliyuli@bupt.edu.cn;

S1. The synthesis method of Au@Ag nanorods.

After preparing gold nanorods, we utilized a seed-mediated growth method to gradually coat their surfaces with a uniform layer of silver, forming silver-coated gold nanorods.

Chemical reagents used in the synthesis process. benzylhexadecyldimethylammonium chloride (CTAC, 99%), L- ascorbic acid (AA, C6H8O6, >99%), Cetyltrimethylammonium bromide (CTAB≥99%), sodium borohydride (NaBH4, 99%), gold (III) chloride trihydrate (HAuCl4·3H2O, >99%), and sodium chloride (NaCl, 99.5%) were used as received. 5,6-Dichloro-2-[[5,6-dichloro-1-ethyl-3-(4-sulfobutyl)-benzimidazol-2-ylidene]-propenyl]-1-ethyl-3-(4-sulfobutyl)-benzimidazolium hydroxide, inner salt, sodium salt (TDBC) was purchased from Few Chemicals and used as received. Deionized water with a resistivity of 18.25 MΩ.cm was used in all experiments.

Figure S1. The high-resolution TEM image of one typical Au@Ag nanocavity.

S2. E-field distribution of Au@Ag nanocavity and mode volume calculation

Figure S2. Electric field distribution of Au@Ag nanorod, calculated by FDTD simulation. (λcav=592 nm) The nanorod was put on the surface of monolayer WS2. The substrate was set as SiO2 and the background was air.

The mode volume of the Au@Ag nanocavity was calculated using the formula1,2:

V=εr|Er|2dVmax⁡(ε(r)|Er|2)

εr represent the environment dielectric constant at r. Considering the plasmon properties, we change the term εr to Re[ε]+2ωImε/γ (ω is the angular frequency of the cavity mode, γ is the Drude damping term. For gold material, γAu~0.07. For silver material, γAg~0.02.)

In a specific calculation, the electric field distributions inside and around the Au and Au@Ag nanorod were calculated at the J-aggregate transition energy (E=2099 meV,λ=592 nm) using the FDTD simulation (Figure S2). Subsequently, the mode volume of Au@Ag nanorod used in our study was calculated to be about 240 nm3.

S3. Calculations of the WS2 exciton resonance

Here, we calculate the WS2 exciton resonance in 200 K-400 K range using O'Donnell Model3,4:

(1)

=2.07 eV represents the excitonic transition energy at 0 K. S=1.78 represents electron-phonon coupling strength. represents the average phonon energy.

Figure S3. The calculated WS2 exciton resonance in 200 K-400 K range.

S4. Absorption measurement of WS2 monolayer

To extract the decay rate of the WS2 excitons, we measured the absorption spectrum of the WS2 monolayer using a typical microscope setup. Firstly, the incident light from a halogen lamp was focused into the sample plane by a 100X magnification objective (NA=0.9). Then, the imaging of the WS2 monolayer was acquired by a color CCD. Finally, the spatial filtering method was used to capture the absorption spectrum of monolayer WS2. As shown in Figure S4, the experimental data agree well with single Lorentz peak fitting results (red line). The WS2 monolayer absorption peak Ex_fit= 2.025 eV, and the exciton width is γx_fit= 26 meV.

Figure S4. The measured absorption spectrum of WS2 monolayer. The red solid line shows the Lorentz fit for the experimental data.

References

1	Zengin, G. et al. Realizing Strong Light-Matter Interactions between Single-Nanoparticle Plasmons and Molecular Excitons at Ambient Conditions. Physical Review Letters 114, 157401, doi:10.1103/PhysRevLett.114.157401 (2015).

2	Wen, J. et al. Room-Temperature Strong Light–Matter Interaction with Active Control in Single Plasmonic Nanorod Coupled with Two-Dimensional Atomic Crystals. Nano Letters 17, 4689-4697, doi:10.1021/acs.nanolett.7b01344 (2017).

3	O’donnell, K.P., Chen, X. Temperature dependence of semiconductor band gaps. Applied physics letters 58, 2924-2926, doi: 10.1063/1.104723 (1991).

4	Cuadra, J. et al. Observation of tunable charged exciton polaritons in hybrid monolayer WS2– plasmonic nanoantenna system. Nano Letters 18, 1777–1785, doi: 10.1021/acs.nanolett.7b04965 (2018).