Supplementary material

Giant enhancement of optical nonlinearity from monolayer MoS2 using plasmonic nanocavity

Liping Hou,1 Haosong Li,1 Qifa Wang,1 Xuetao Gan, 1, * Fajun Xiao1, * and Jianlin Zhao1, *

1 Key Laboratory of Light Field Manipulation and Information Acquisition, Ministry of Industry and Information Technology, and Shaanxi Key Laboratory of Optical Information Technology, School of Physical Science and Technology, Northwestern Polytechnical University, Xi’an 710129, China

* Correspondence E-mail: xuetaogan@nwpu.edu.cn; fjxiao@nwpu.edu.cn; jlzhao@nwpu.edu.cn.

Content

S1. Optical setup for nonlinear optical measurements.

S2. SEM and dark-field images of the MoS2-DoMN.

S3. Calculations of SHG and THG from the monolayer MoS2-DoMN.

S4: SHG and THG from 3 other MoS2-DoMN hybrid structures.

S5. Effective enhancement factor.

S6. Polarization-resolved scattering spectra.

S7: SHG far-field amplitude patterns; phase differences (|MoS2-DoMN|) of the SHG far-field between MoS2 and DoMN in the xz-plane.

S8. Calculation of the parallel components of the SHG and THG intensities.

S1: Optical setup for nonlinear optical measurements

Figure S1: Optical setup for nonlinear optical measurements. L: lens, HWP: half-wave plate, PH: pinhole, DM: dichroic mirrors, FM: flip-mirror, A: analyzer, Obj: objective lens.

S2. SEM and dark-field images of the MoS2-DoMN.

Figure S2: (A) SEM and (B) dark-field images of the MoS2-DoMN. The dashed circle indicates actual detection area. The inset of (A) shows the zoom-in SEM image of Au nanosphere dimer, where the scale bar is 100nm.

S3. Calculations of SHG and THG from the monolayer MoS2-DoMN.

The initial step involved in determining the field distribution Er,ω of MoS2-DoMN at the fundamental frequency using COMSOL based on the finite element method. Subsequently, the second- and third-order nonlinear polarizations of the monolayer MoS2 and DoMN were derived from P(2)r,2ω=χ(2)Er,ωEr,ω and P(3)r,3ω=χ(3)Er,ωEr,ωEr,ω. Considering the monolayer MoS2 belongs to the D3h point group, χ(2) possesses a single non-zero element χ(2)≡χyyy2=-χxxy2=-χxyx2=-χyxx2, and χ(3)comprises the non-zero elements as follows: χyyyy3=χxxxx3=χyyxx3+χyxxy3+χyxyx3,χyyxx3=χxxyy3,   χxyyx3=χyxxy3, and χxyxy3=χyxyx3. Assuming the excitation with arbitrary polarization Er,ω=Er,ωxcos⁡(θ)±iysin(θ), the second- and third-order nonlinear polarization of monolayer MoS2 can be described by

PMoS2(2)r,ω=ε0χyyy2Er,ω2∓sin2θx-y,              (1)

and

PMoS2(3)r,ω=ε0χyyyy3Er,ω3xcos⁡(θ)±iysin(θ)cos2θ,        (2)

where ε0  is the vacuum permittivity, χyyy2 and χyyyy3 are taken from the experimental data as 2.2 pmV-1 and  10-17 m2V-2 [1]，respectively. For the metallic part of the hybrid structure, the second-order surface susceptibility of Au is dominated by the component χ⊥⊥⊥2. As a result, the corresponding nonlinear polarization is written as

PAu(2)r,ω=χ⊥⊥⊥2E⊥r,ωE⊥r,ωE⊥r,ω,                (3)

where χ⊥⊥⊥2 was set as 40 pmV-1 [2]. The general expression for the third-order nonlinear polarization of Au structure is denoted as

PAu(3)r,ω=χAu3Er,ωEr,ωEr,ω,                  (4)

where χAu3 was taken as  3.4×10-16 m2V-2 [3].The nonlinear polarizations calculated from Eq. (1)-(4) were then considered as the SHG and THG sources of the MoS2-DoMN hybrid structure, which was executed by the finite element solver to obtain the nonlinear signals at TH and SH frequencies. The radiation patterns were derived using the far-field domain module.

S4: SHG and THG from 3 other MoS2-DoMN hybrid structures.

Figure S3: (A)-(C) Full views of bright-field (left panels) and SEM (right panels) for the three MoS2-DoMN hybrid structures. The inset of (right panels) shows the Au nanosphere dimer, where the scale bar is 100 nm. (D)-(F) Measured scattering spectra, (G)-(I) SHG and THG spectra of the three MoS2-DoMNs.

Table S1: Summary of SHG and THG EF.

| MoS2-DoMN |  | 1 | 2 | 3 | 4 | averaged |
| --- | --- | --- | --- | --- | --- | --- |
| EF | SHG | 15 | 9 | 17 | 12 | 13 |
|  | THG | 68 | 65 | 64 | 62 | 65 |

S5. Effective enhancement factor.

Considering that the collected nonlinear signals also include contributions from the background MoS2, the actual nonlinear responses of MoS2 enhanced by the DoMN should be large. To quantify the real nonlinearity enhanced by the DoMN, we define the effective enhancement factor EFe as

EFe=Idim-I0-Idim0I0S0Sdim                                 (5)

where Idim, I0, and Idim0 are the SHG/THG intensities of the MoS2-DoMN hybrid structure, pristine monolayer MoS2, and the DoMN, respectively. Sdim denotes the area of the dimer (∼0.03μm2) and S0 represents the area of MoS2 we collected (∼6μm2). According to Eq. (5), the enhancement factors are determined to be 3000- and 13600-folds for the SHG and THG of MoS2, respectively.

Table.S2: Comparisons of THG and SHG EFe.

| Structure | SHG EFe | THG EFe | FW/nm | Ref. |
| --- | --- | --- | --- | --- |
| WS2/NCOM | 280 | \ | 800 | [4] |
| WSe2/trenches | 7000 | \ | 800 | [5] |
| WS2/nanogroove | 400 | \ | 860 | [6] |
| WS2/nanoantenna | 40 | \ | 1260 | [7] |
| WS2/NPoM | 3000 | 3800 | 1240/1260 | [8] |
| MoS2/nanohole | 1527 | \ | 869.6 | [9] |
| MoS2/NW | 140 | \ | 800 | [10] |
| WSe2/NPOM | 3800 | \ | 1450 | [11] |
| MoS2(GR)/QD coating | 170 | 60 | 820/1350 | [12] |
| MoS2/DoMN | 3000 | 13600 | 1550 | This work |

\ not available.

S6. Polarization-resolved scattering spectra.

Figure S4: (A) Polarization-resolved scattering spectra of MoS2-DoMN. The SH and TH frequencies are marked with red and black dashed lines, respectively. Polarization dependence of the (B) SH and (C) TH frequencies, respectively.

S7: SHG far-field amplitude patterns and phase differences (|MoS2-DoMN|) of the SHG far-field between MoS2 and DoMN in the xz-plane.

Figure S5: (A) SHG far-field amplitude patterns of the monolayer MoS2 (blue solid curves), the DoMN (green solid curves) and the MoS2-DoMN (red solid curves) in the xz-plane. (B) Phase differences (|MoS2-DoMN|) of the SHG far-field between MoS2 and DoMN in the xz-plane.

S8: Calculation of the parallel components of the SHG and THG intensities

The polarization dependence of SHG for pristine MoS2 and MoS2-DoMN in Figure 3(E) can be described as [6]:

IMoS2(2)∝χyyy2cos⁡(2θ+3θ0)2                          (6)

and

I(2)∝χyyy2cos2θ-c0sin2θcos3θ0-c0sin2θsin3θ0                   (7)

where c0 is the coupling coefficient of the pump laser with the dimer, θ is the angle between the pump laser and the dimer long axis and θ0 is the mismatch angle between the armchair (γ) direction and the dimer axis (about 3.13° for the measured sample).

The parallel components THG intensities of the pristine MoS2 and MoS2-DoMN in Figure 3(F) could be described as:

IMoS2(3)∝Asinθ+2θ0+Bsin⁡(θ+θ0)2                       (8)

and

I(3)∝Acos2θ+c02sin2θcosθ+Bcosθ+Csinθ+θ02                (9)

where A, B and C contain all of the nonzero elements in the third-order susceptibility tensor (χyyyy3).

References

[1]	A. Saynatjoki, L. Karvonen, H. Rostami, A. Autere, S. Mehravar, A. Lombardo, R. A. Norwood, T. Hasan, N. Peyghambarian, H. Lipsanen, K. Kieu, A. C. Ferrari, M. Polini, and Z. Sun, "Ultra-strong nonlinear optical processes and trigonal warping in MoS2 layers," Nat. Commun., vol. 8, no. 1, pp. 893, 2017.

[2]	Y. Uchiho, M. Shimojo, and K. Kajikawa, "Electro-optic effect and optical rectification in gold nanoparticles immobilized above a gold surface," J. Phys. D: Appl. Phys., vol. 43, pp. 495101, 2010.

[3]	D. Compton, L. Cornish, and E. v. d. Lingen, "The third order nonlinear optical properties of gold nanoparticles in glasses, part II," Gold Bull., vol. 36, no. 2, pp. 51-58, 2003.

[4]	X. Han, K. Wang, P. D. Persaud, X. Xing, W. Liu, H. Long, F. Li, B. Wang, M. R. Singh, and P. Lu, "Harmonic resonance enhanced second-harmonic generation in the monolayer WS2-Ag nanocavity," ACS Photonics, vol. 7, no. 3, pp. 562-568, 2020.

[5]	Z. Wang, Z. Dong, H. Zhu, L. Jin, M. H. Chiu, L. J. Li, Q. H. Xu, G. Eda, S. A. Maier, A. T. S. Wee, C. W. Qiu, and J. K. W. Yang, "Selectively plasmon-enhanced second-harmonic generation from monolayer tungsten diselenide on flexible substrates," ACS Nano, vol. 12, no. 2, pp. 1859-1867, 2018.

[6]	J. Shi, W.-Y. Liang, S. S. Raja, Y. Sang, X.-Q. Zhang, C.-A. Chen, Y. Wang, X. Yang, Y.-H. Lee, H. Ahn, and S. Gwo, "Plasmonic enhancement and manipulation of optical nonlinearity in monolayer tungsten disulfide," Laser Photonics Rev., vol. 12, no. 10, pp. 1800188, 2018.

[7]	F. Spreyer, C. Ruppert, P. Georgi, and T. Zentgraf, "Influence of plasmon resonances and symmetry effects on second harmonic generation in WS2-plasmonic hybrid metasurfaces," ACS Nano, vol. 15, no. 10, pp. 16719-16728, 2021.

[8]	J. Shi, Z. Lin, Z. Zhu, J. Zhou, G. Q. Xu, and Q. H. Xu, "Probing excitonic rydberg states by plasmon enhanced nonlinear optical spectroscopy in monolayer WS2 at room temperature," ACS Nano, vol. 16, no. 10, pp. 15862-15872, 2022.

[9]	Q. Leng, H. Su, J. Liu, L. Zhou, K. Qin, Q. Wang, J. Fu, S. Wu, and X. Zhang, "Enhanced second-harmonic generation in monolayer MoS2 on suspended metallic nanostructures by plasmonic resonances," Nanophotonics, vol. 10, no. 7, pp. 1871-1877, 2021.

[10]	D. Li, C. Wei, J. Song, X. Huang, F. Wang, K. Liu, W. Xiong, X. Hong, B. Cui, A. Feng, L. Jiang, and Y. Lu, "Anisotropic enhancement of second-harmonic generation in monolayer and bilayer MoS2 by integrating with TiO2 nanowires," Nano Lett., vol. 19, no. 6, pp. 4195-4204, 2019.

[11]	T. Zhang, Q. Guo, Z. Shi, S. Zhang, and H. Xu, "Coherent second harmonic generation enhanced by coherent plasmon-exciton coupling in plasmonic nanocavities," ACS Photonics, vol. 10, no. 5, pp. 1529-1537, 2023.

[12]	H. Hong, C. Wu, Z. Zhao, Y. Zuo, J. Wang, C. Liu, J. Zhang, F. Wang, J. Feng, H. Shen, J. Yin, Y. Wu, Y. Zhao, K. Liu, P. Gao, S. Meng, S. Wu, Z. Sun, K. Liu, and J. Xiong, "Giant enhancement of optical nonlinearity in two-dimensional materials by multiphoton-excitation resonance energy transfer from quantum dots," Nat. Photonics, vol. 15, no. 7, pp. 510-515, 2021.