Polarization Spatial Diversity and Multiplexing MIMO Surface Enabled by Graphene for Terahertz Communications

Jianzhou Huang1,2, Xudong Wu1,2, Chenjie Xiong1,2, Jia Zhang1, 2,3, and Bin Hu1,2*

1. School of Optics and Photonics, Beijing Institute of Technology, Beijing 100081, China.

2. National Key Laboratory on Near-surface Detection, Beijing, 100072, China.

3. China Academy of Aerospace Science and Innovation, Beijing 100089, China.

*Correspondence and requests for materials should be addressed to B. H (E-mail: hubin@bit.edu.cn)

Table S1: Selected Unit cells

| No. | θ (°) | β (°) | Ey Phase (π) |
| --- | --- | --- | --- |
| Superlattice 1 (N=8) |  |  |  |
| 1 | 20 | 45 | 2.06 |
| 2 | 70 | 45 | 1.8 |
| 3 | 110 | 45 | 1.55 |
| 4 | 140 | 45 | 1.32 |
| 5 | 190 | 45 | 1.05 |
| 6 | 70 | -45 | 0.8 |
| 7 | 110 | -45 | 0.55 |
| 8 | 140 | -45 | 0.32 |
| Superlattice 2 (N=18) |  |  |  |
| 1 | 20 | 45 | 2.06 |
| 2 | 40 | 45 | 1.95 |
| 3 | 60 | 45 | 1.85 |
| 4 | 80 | 45 | 1.74 |
| 5 | 100 | 45 | 1.63 |
| 6 | 120 | 45 | 1.46 |
| 7 | 140 | 45 | 1.32 |
| 8 | 160 | 45 | 1.21 |
| 9 | 180 | 45 | 1.1 |
| 10 | 20 | -45 | 1.06 |
| 11 | 40 | -45 | 0.95 |
| 12 | 60 | -45 | 0.85 |
| 13 | 80 | -45 | 0.74 |
| 14 | 100 | -45 | 0.63 |
| 15 | 120 | -45 | 0.46 |
| 16 | 140 | -45 | 0.32 |
| 17 | 160 | -45 | 0.21 |
| 18 | 180 | -45 | 0.1 |

Figure S1: Absorption of different unit cell structures under different graphene chemical potentials (f=0.289 THz).

Figure S2: Electrical isolation measurement between different graphene regions. (a)-(f) Electrical isolation between graphene-covered metasurfaces CH1-CH4. (g)-(h) Conductivity between the electrode and graphene.

Electrical isolation between metasurface CH1-CH4 was measured as shown in Figure S2(a)-(f), confirming mutual isolation across all four metasurface pairs. This demonstrates that alcohol-swab wiping effectively achieves graphene segmentation and electrical isolation. Additionally, electrode-to-graphene conductivity measurements (Figure S2(g)-(h)) were performed using red and black probes contacting the electrode and off-metasurface graphene, respectively. The results indicate conductive behavior between the electrode and graphene, with resistance ranging from 2 to 3 kΩ.

Figure S3: Sensitivity to misalignment. Calculated based on the data of radiation patterns.

Figure S4: (a) Output ASCII code data by Raspberry Pi. (b) Received ASCII code data with interference. (c) Decoded results of the x-polarization (Rx) and y-polarization (Ry) channels, respectively. Rc is the

Sy and Sx are the text data transmitted simultaneously through the Cy1 and Cx1 channels. Figure S4(a) shows the output of Raspberry Pi. Same as in the above experiment, we used the metal plate that randomly blocks Cy1 and Cx1 channels when transmitting text data to simulate the situation of communication interruption during directional communication. As depicted in Figure S4(b), the correct information of 'B' was lost in the communication over the Cx1 channel. Meanwhile, the identification code ‘010’ was also lost. In this case, the ASCII code ‘00000000’ was used to replace this whole 8-bit byte, which is the null character ‘NUL’ in ASCII code. Nevertheless, the correct data (01000010) in the Cy1 channel can be used for text restoration. The correct ASCII code for "B" can be obtained by performing logical OR (00000000 || 01000010 = 01000010). Figure S4(c) demonstrates the restoration through the polarization spatial diversity. Rx and Ry are text transmitted separately under communication interference, resulting in incorrect restoration. However, the correct text information can be recovered by performing the logical operation of OR on the data transmitted through two channels, as depicted in Rc.