Supporting Material for

Second-harmonic generation in NbOI2-integrated silicon nitride 
microdisk resonators

Ning Liu1,2, Qiang Liu1,2, Yutian Lin1,2, Zhihong Zhu 1,2,*, and Ken Liu1,2,*

1College of Advanced Interdisciplinary Studies & Hunan Provincial Key Laboratory of Novel Nano-Optoelectronic Information Materials and Devices, National University of Defense Technology, Changsha 410073, China.

2 Nanhu Laser Laboratory, National University of Defense Technology, Changsha 410073, China.

*Corresponding authors: Zhihong Zhu, zzhwcx@163.com, Ken Liu, liukener@163.com

Table of Content

Note S1: Robustness and versatility of phase matching technology by designing geometry

Note S2: Analysis of SHG conversion efficiency

Figure S1: Acquisition of 2D NbOI2

Figure S2: Optical absorption spectrum of 2D NbOI2 and corresponding αhν1/2-hν plot

Figure S3: Stability of 2D NbOI2 under ambient conditions

Figure S4: Schematic illustrations of the atomic structure of NbOI2

Figure S5: Fabrication process flow of the suspended Si3N4 microdisks

Figure S6: Wet etching rate of SiO2

Figure S7: OM image of a typical Si3N4 microdisk used in the experiment

Figure S8: OM images of the 2D NbOI2 and the PVA/NbOI2/Si3N4 microdisk heterostructure

Figure S9: Phase matching analysis of a Si3N4 microdisk resonator integrated with 30nm-thick NbOI2 flake.

Figure S10: Raw transmission spectrum of the Si3N4 microdisk integrated with NbOI2 at 1540-1560 nm.

Figure S1. Acquisition of 2D NbOI2. (a) Optical image of bulk NbOI2 crystals. (b) Optical microscopy (OM) image of 2D NbOI2 flakes obtained via mechanical exfoliation. (c) Atomic force microscopy (AFM) image corresponding to the NbOI2 flakes in (b). (d) Height profile along the white dashed line in (c), indicating a thickness of ~16 nm for the NbOI2 flake.

Figure S2. Optical absorption spectrum of 2D NbOI2 and corresponding αhν1/2-hν plot. (a) Optical absorption spectrum of a 80 nm-thick NbOI2 flake. Inset: OM image of the sample for absorption measurement, with the blue circle marking the tested region. Scale bar: 5 μm. (b) αhν1/2-hν plot derived from the absorption spectrum in (a) (purple shaded area denotes the linear fitting region), yielding a bandgap of ~1.92 eV for the 90 nm-thick NbOI2 flake.

Figure S3. Stability of 2D NbOI2 under ambient conditions. (a) AFM image of the 2D NbOI2 in Figure 1c. (b) Height profile along the white dashed line in (a), indicating a thickness of ~30 nm. (c) OM images of time-dependent degradation of the NbOI2 flake under ambient conditions (~60% relative humidity).

Figure S4. Schematic illustrations of the atomic structure of NbOI2. (a) Side view of the NbOI₂ structure along the c-axis, showing an alternation in Nb–Nb distances. (b) Side view along the b-axis, highlighting alternating variations in Nb–O bond lengths.

Figure S5. Fabrication process flow of the suspended Si3N4 microdisks. (a) Deposition of a Si3N4 thin film on a SiO2/Si substrate. (b) Spin-coating of photoresist. (c) Lithography for microdisk patterning. (d) Dry etching to transfer the pattern to the Si3N4 layer. (e) Wet etching of SiO2 to release the Si3N4 microdisks.

Figure S6. Wet etching rate of SiO2. (a) Test results of surface-to-substrate height on the Si3N4 microdisk before (blue line) and after (red line) 8 hours of wet etching, demonstrating a SiO₂ etching rate of ~100 nm/h. The etching was performed with 1/3 mol/L KOH solution under an 80°C water bath. (b) OM image of the Si3N4 microdisk. The height difference between the upper surface of Si3N4 microdisk and the substrate is about 2 μm, and the diameter of the microdisk is 40 μm.

Figure S7. OM image of a typical Si3N4 microdisk used in the experiment. Inset: The white line indicates the height difference (~3.2 μm) between the top surface of the SiN microdisk and the substrate.

Figure S8. (a) OM image for the 2D NbOI2 in Figure 2c. (b) OM image of the PVA/NbOI2/ Si3N4 microdisk heterostructure.

Figure S9. Effective refractive index (neff) curves of the TE0 mode at the fundamental frequency (ωP-TE0, blue line) and the TM3 mode at the second harmonic frequency (ωSHG-TM3, orange line) as functions of the microdisk diameter for a Si3N4 microdisk integrated with a 30 nm-thick NbOI2 flake. The intersection at a radius of ~19.6 μm indicates the phase-matching point. Insets: Electric field distributions of the TE0 (fundamental frequency) and TM3 (second-harmonic frequency) modes.

Figure S10. Raw transmission spectrum of the Si3N4 microdisk integrated with NbOI2 at 1540-1560 nm, where the two resonant wavelengths studied in Figure 3 are marked with red circles.

Note S1: Robustness and versatility of phase matching technology by designing geometry

The phase-matching achieved through photonic design is indeed highly versatile and serves as a powerful tool for engineering a wide range of nonlinear processes.

(1) Different nonlinear spectroscopic techniques (e.g., pump-probe, double quantum coherence) require specific phase-matching conditions. In bulk optics, this is controlled by the alignment of the wavevectors of the free-space beams. In our integrated microcavity platform, an analogous, but far more precise, control is achieved by designing the geometry (e.g., radius, waveguide width, and etch depth) to tailor the dispersion of the optical modes. This allows us to target the specific resonance conditions required for a desired nonlinear process: for sum-frequency generation (SFG), the cavity can be designed to support three resonant modes satisfying ω3=ω1+ω2 and m3 = m1+m2; for difference-frequency generation (DFG), the conditions would be ω3=ω1-ω2 and m3 = m1 - m2; for pump-probe experiments, the same principle applies. The cavity can be engineered to resonate at both the pump and probe wavelengths, dramatically enhancing the interaction strength for sensitive measurements like cross-phase modulation or two-photon absorption.

Therefore, the photonic design is not limited to SHG; it is a general-purpose methodology for achieving phase-matching in a vast landscape of χ(2)and χ(3) nonlinear optics.

(2) Robustness and Post-Fabrication Tuning. Once fabricated, the phase-matching condition is inherently stable and locked into the device geometry, immune to mechanical vibrations or misalignment, which is a significant advantage over free-space setups. While the fundamental phase-matching is set by geometry, several post-fabrication tuning techniques are well-established to compensate for manufacturing tolerances or to actively switch between processes, such as “thermal tuning”, “carrier-effect tuning”, “strain tuning” and so on. These methods allow for fine-tuning the phase-matching condition with high precision, making the platform both robust and adaptable.

Note S2: Analysis of SHG conversion efficiency

We have employed nonlinear coupled-mode theory to estimate the maximum achievable SHG efficiency in the NbOI2-integrated Si3N4 microdisk system.

The SHG process in a microdisk resonator involves two optical modes: mode a at the fundamental frequency (with angular frequency ω) and mode b at the second-harmonic frequency (with angular frequency ωb ≈ 2ωa). When the angular frequency of the pump light ωp approaches ωa, the microdisk system can be described by the following Hamiltonian [S1]:

|  | H=ωaa*a+ωbb*b+ga*2b+a2b*+εpaeiωpt+a*e-iωpt), | (1) |
| --- | --- | --- |

Where, a and b represent the Bosonic operators for the fundamental mode and second-harmonic mode, respectively; εp=2κa,1Ppℏωp represents the pump field strength, Pp is the pump power, κa,1 is the external coupling rate between mode a and the coupling waveguide, g is the nonlinear coupling strength between mode a and mode b:

|  | ℏg=ε0dθ dr dz 3χ2r42ua,z*r2ub,zr, | (2) |
| --- | --- | --- |

where ε0 is the vacuum permittivity, χ2r denotes the second-order susceptibility of the medium, uab,zr represents the electric field profiles of mode a(b) within the microdisk resonator, expressed in polar coordinates.

Next, we introduce the effective mode overlap factor:

|  | ζ=dr dz ua,z*r,z2ub,zr,zdr dz ua,zr,z2dr dz ub,zr,z2. | (3) |
| --- | --- | --- |

So

|  | g≈ζℏωa2ωbε02πR⋅1εaεb⋅3χ242×δmb-2ma, | (4) |
| --- | --- | --- |

where εa(b) represents the relative permittivity of mode a(b), which depends on the angular frequency and spatial position; ma(mb) denotes the angular momentum of mode a(b). For the Kronecker delta function δ(mb - 2ma), the coupling strength g assumes a non-zero value only when momentum conservation condition mb - 2ma = 0 is satisfied.

Under CW pumping conditions, using the non-depletion approximation, the SHG conversion efficiency can be expressed in the following form:

|  | η=PSHGPp2=g22κb,1δb2+κb22κa,1δa2+κa22ℏωbℏωp2. | (5) |
| --- | --- | --- |

where δa = ωa - ωp (δb = ωb - 2ωp) represents the angular frequency detuning of mode a(b) relative to the pump; κa = κa,1 + κa,0 (κb = κb,1 + κb,0) denotes the total loss rate of cavity mode a(b), specifically including the external loss rate κa(b),1 and the intrinsic loss rate κa(b),0. When the pump frequency is tuned to match the frequency of cavity mode a, δa = ωa - ωp = 0; when the energy conservation condition is satisfied in the SHG process, i.e., ωb ≈ 2ωa, δb = ωb - 2ωp = 0 is automatically satisfied, indicating that the double-resonance condition is met in the second-harmonic conversion process.

At this point, η can be further simplified to:

|  | η=16g2κb,0κb,1+κb,12κa,0κa,1+κa,14⋅1ℏωp. | (6) |
| --- | --- | --- |

Furthermore, when both modes satisfy the critical coupling condition, i.e., κa,1 = κa,0，κb,1 = κb,0, the maximum SHG conversion efficiency can be expressed as:

|  | ηmax=g24κb,0κa,02⋅1ℏωp=g2Qa,02Qb,0ℏωa4. | (7) |
| --- | --- | --- |

where Qa,0=ωa2κa,0，Qb,0=ωb2κb,0 represent the intrinsic Q factors of modes a and b.

Under the phase matching analysis of the microdisk shown in Figure 2(f), energy and momentum conservation are satisfied. Assuming the nonlinear coupling strength g remains constant, subsequent experimental optimizations can increase the intrinsic quality factor of the microcavity by two orders of magnitude (the intrinsic Q of the bare Si3N4 microcavity rises from ~10⁴ to ~10⁶, with corresponding estimated Qa,0 and Qb,0 also improving by two orders of magnitude). Under critical coupling conditions, the SHG conversion efficiency can be improved to 24,000 %/W. This value exceeds the highest reported in comparable works (as listed in Table 1) by two orders of magnitude, demonstrating the significant application potential of our proposed NbOI2-integrated Si3N4 microdisk resonator in the field of integrated second-order nonlinear optics.

Reference

[S1] X. Guo, C.-L. Zou, and H. X. Tang, "Second-harmonic generation in aluminum nitride microrings with 2500%/W conversion efficiency," Optica, vol. 3, no. 10, pp. 1126-1131, 2016.