Supplementary Information for 
Thienothiophene-Benzotriazole Based Semi-crystalline Linear Copolymers for Organic Field Effect Transistors
Seungjib Yum,1 Tae Kyu An,2 Xiaowei Wang,1 Mohammad Afsar Uddin,1 Thanh Luan Nguyen,1 Shuhao Xu,1 Hwasook Ryu,1 Yu Jin Kim,2 Sungu Hwang,1 Chan Eon Park,*,2 and Han Young Woo*, 1
1Department of Nanofusion Engineering, Department of Cogno-Mechatronics Engineering, Pusan National University, Miryang, 627-706, Republic of Korea. Fax: +82-55-350-5279; Tel: +82-55-350-5300; E-mail: hywoo@pusan.ac.kr

2POSTECH Organic Electronics Laboratory, Polymer Research Institute, Department of Chemical Engineering, Pohang University of Science and Technology, Pohang, Gyungbuk 790-784, South Korea. Fax: +82-54-279-8298; Tel: +82-54-279-2269; E-mail: cep@postech.ac.kr
[image: image1.jpg]Heat flow (W/g)

——PTTBTz
——PTTBTzF
——PTTBTz-OR

100 200 300 400 500

Temperature (°C)

100

60

40

(%) yB1am




Figure S1. TGA and DSC thermograms of polymers.
[image: image2.png]Y

R

Normalized Absorbance

1.0
0.8
0.6
0.4
02

0.0
3

G

°

Normalized Absorbance

1.0
08
0.6
0.4
0.2

0.0

—as-casted
—230°C
—280°C
—340°C
——400°C

PTTBTz-F

Normalized Absorbance

1.0

08

0.6

0.4

0.2

0.0

PTTBTz-OR

as-casted
——120°C
—170°C
——230°C
——290°C

PTTBTz —as-casted
—130°C
—170°C
—230°C
00 400 500 600 700 800

Wavelength (nm)

3

00 400 500 600 700

Wavelength (nm)

800

3

00 400 500 600 700

Wavelength (nm)

800




Figure S2. Normalized UV-vis absorption spectra of (a) PTTBTz, (b) PTTBTz-F and (c) PTTBTz-OR with changing the annealing temperature. 
[image: image3.jpg]Current (a.u.)

—PTTBTz
—PTTBTzF
— PTTBTz-OR

0.5 1.0 1.5
Potential E(V) vs. F¢/Fc’




Figure S3. Cyclic voltammogram for BTz-based polymers.

S3

