# Supplementary Material

Table S1. Surface Area and Porosity Properties of Adsorbents

| Material | BET Surface Area (m²/g) | Pore Volume (cm³/g) | Average Pore Diameter (nm) | Micropore Volume (cm³/g) |
| --- | --- | --- | --- | --- |
| AC | 1,110 ± 15 | 0.61 ± 0.02 | 2.20 ± 0.05 | 0.42 ± 0.01 |
| AC-ZnO/Al₂O₃ | 1,247 ± 18 | 0.68 ± 0.03 | 2.18 ± 0.04 | 0.38 ± 0.02 |

Table S2. EDS Elemental Analysis of AC-ZnO/Al₂O₃ Composite

| Element | Atomic % | Weight % |
| --- | --- | --- |
| C | 78.5 ± 1.2 | 72.1 ± 1.1 |
| O | 12.3 ± 0.8 | 15.1 ± 0.9 |
| Zn | 4.6 ± 0.3 | 7.3 ± 0.4 |
| Al | 4.2 ± 0.2 | 5.4 ± 0.3 |
| Others | 0.4 ± 0.1 | 0.1 ± 0.1 |

Table S3. Kinetic Parameters for DBT Adsorption on AC-ZnO/Al₂O₃ Composite

| Kinetic Model | Parameter | Value | Units |
| --- | --- | --- | --- |
| Experimental | qₑ,exp | 58.4 ± 1.2 | mg/g |
| Pseudo-first-order | qₑ,cal | 51.2 ± 2.1 | mg/g |
|  | k₁ | 0.0156 ± 0.0008 | min⁻¹ |
|  | R² | 0.952 | - |
|  | χ² | 12.34 | - |
| Pseudo-second-order | qₑ,cal | 59.1 ± 1.4 | mg/g |
|  | k₂ | 0.00048 ± 0.00003 | g/mg·min |
|  | h₀ | 1.68 ± 0.08 | mg/g·min |
|  | R² | 0.998 | - |
|  | χ² | 1.87 | - |

Table S4. Isotherm Parameters for DBT Adsorption

| Isotherm Model | Parameters | AC | AC-ZnO/Al₂O₃ |
| --- | --- | --- | --- |
| Langmuir | qₘ (mg/g) | 35.2 ± 1.1 | 58.7 ± 1.5 |
|  | KL (L/mg) | 0.042 ± 0.003 | 0.089 ± 0.005 |
|  | R² | 0.988 | 0.995 |
| Freundlich | KF (mg/g)(L/mg)^(1/n) | 8.7 ± 0.4 | 15.3 ± 0.6 |
|  | n | 2.8 ± 0.1 | 3.2 ± 0.2 |
|  | R² | 0.945 | 0.962 |

Table S5. Thermodynamic Parameters for DBT Adsorption

| Temperature (K) | ΔG° (kJ/mol) | ΔH° (kJ/mol) | ΔS° (J/mol·K) |
| --- | --- | --- | --- |
| 298 | -10.2 ± 0.3 | -23.7 ± 1.2 | -45.2 ± 2.1 |
| 308 | -9.7 ± 0.4 |  |  |
| 318 | -9.2 ± 0.3 |  |  |
| 328 | -8.8 ± 0.5 |  |  |

Table S6. Competitive Adsorption in Multi-component Systems

| Pollutant | Single Component qₑ (mg/g) | Multi-component qₑ (mg/g) | Reduction (%) |
| --- | --- | --- | --- |
| Pb²⁺ | 52.4 ± 1.3 | 47.6 ± 1.2 | 9.2 |
| Phenol | 94.7 ± 2.1 | 87.4 ± 1.8 | 7.7 |
| Methylene Blue | 26.8 ± 0.6 | 23.2 ± 0.4 | 13.4 |

Table S7. Regeneration Performance of AC-ZnO/Al₂O₃ Composite

| Cycle | DBT Capacity (mg/g) | Capacity Retention (%) | Pb²⁺ Removal (%) | Efficiency Retention (%) |
| --- | --- | --- | --- | --- |
| 1 | 58.7 ± 1.5 | 100.0 | 95.2 ± 1.1 | 100.0 |
| 2 | 56.2 ± 1.4 | 95.7 | 93.1 ± 1.0 | 97.8 |
| 3 | 53.8 ± 1.3 | 91.6 | 90.7 ± 0.9 | 95.3 |
| 4 | 51.4 ± 1.2 | 87.6 | 88.2 ± 1.1 | 92.6 |
| 5 | 49.9 ± 1.1 | 85.0 | 78.1 ± 1.2 | 82.0 |

Table S8. Real Crude Oil Desulfurization Results

| Parameter | Initial Value | Final Value | Removal Efficiency (%) |
| --- | --- | --- | --- |
| Total Sulfur (ppm) | 1,247 ± 25 | 187 ± 12 | 85.0 ± 1.8 |
| DBT (mg/L) | 145 ± 8 | 28 ± 3 | 80.7 ± 2.1 |
| Benzothiophene (mg/L) | 89 ± 5 | 15 ± 2 | 83.1 ± 1.9 |
| 4,6-DMDBT (mg/L) | 76 ± 4 | 18 ± 2 | 76.3 ± 2.3 |

Table S9. Municipal Sewage Treatment Results

| Parameter | Initial Value | Final Value | Removal Efficiency (%) |
| --- | --- | --- | --- |
| COD (mg/L) | 324 ± 18 | 71 ± 6 | 78.2 ± 2.1 |
| BOD₅ (mg/L) | 189 ± 12 | 35 ± 4 | 81.5 ± 1.9 |
| Total Pb (mg/L) | 0.18 ± 0.02 | 0.02 ± 0.003 | 88.9 ± 3.1 |
| Total Phenols (mg/L) | 2.4 ± 0.3 | 0.4 ± 0.1 | 83.3 ± 2.8 |
| Turbidity (NTU) | 45 ± 3 | 8 ± 1 | 82.2 ± 2.4 |

Table S10. Complete XRD Peak Assignment for AC-ZnO/Al₂O₃ Composite

| 2θ (°) | d-spacing (Å) | Phase | Miller Index (hkl) | Intensity (%) | FWHM (°) |
| --- | --- | --- | --- | --- | --- |
| 23.5 | 3.78 | Carbon | (002) | 45.2 | 1.85 |
| 25.6 | 3.47 | Al₂O₃ | (012) | 28.4 | 0.42 |
| 31.7 | 2.82 | ZnO | (100) | 62.8 | 0.38 |
| 34.4 | 2.60 | ZnO | (002) | 89.5 | 0.35 |
| 35.1 | 2.55 | Al₂O₃ | (104) | 41.2 | 0.46 |
| 36.2 | 2.48 | ZnO | (101) | 100.0 | 0.36 |
| 37.8 | 2.38 | Al₂O₃ | (110) | 35.7 | 0.48 |
| 43.2 | 2.09 | Carbon | (100) | 22.1 | 2.15 |
| 43.4 | 2.08 | Al₂O₃ | (113) | 29.8 | 0.51 |
| 47.5 | 1.91 | ZnO | (102) | 42.6 | 0.41 |
| 52.5 | 1.74 | Al₂O₃ | (024) | 18.9 | 0.55 |
| 56.6 | 1.62 | ZnO | (110) | 38.4 | 0.43 |
| 57.5 | 1.60 | Al₂O₃ | (116) | 22.1 | 0.58 |
| 62.8 | 1.48 | ZnO | (103) | 29.7 | 0.48 |
| 66.5 | 1.40 | Al₂O₃ | (214) | 15.6 | 0.62 |
| 67.9 | 1.38 | ZnO | (112) | 25.3 | 0.52 |

Table S11. Particle Size Distribution Analysis from SEM Images

| Size Range (nm) | Frequency (%) | ZnO Particles | Al₂O₃ Particles |
| --- | --- | --- | --- |
| 10-15 | 12.4 | 8.2 | 18.6 |
| 15-20 | 28.7 | 31.5 | 24.8 |
| 20-25 | 35.2 | 38.7 | 31.2 |
| 25-30 | 18.9 | 16.8 | 21.4 |
| 30-35 | 4.8 | 4.8 | 4.0 |

Table S12. Detailed FTIR Peak Assignments

| Wavenumber (cm⁻¹) | Assignment | Material | Intensity |
| --- | --- | --- | --- |
| 3445 | O-H stretching | AC | Strong |
| 3382 | O-H stretching (Al-OH) | Composite | Medium |
| 2924 | C-H stretching | AC, Composite | Weak |
| 2854 | C-H stretching | AC, Composite | Weak |
| 1635 | C=C aromatic stretching | AC, Composite | Strong |
| 1580 | C=C aromatic stretching | AC, Composite | Medium |
| 1384 | C-H bending | AC, Composite | Medium |
| 1052 | Metal-O-C interface bonds | Composite | Medium |
| 798 | Al-O stretching | Composite | Strong |
| 642 | Al-O-Al bending | Composite | Medium |
| 561 | Zn-O stretching | Composite | Strong |
| 468 | Zn-O stretching | Composite | Medium |

Table S13. Thermal Decomposition Stages

| Temperature Range (°C) | Weight Loss (%) | Process | Material |
| --- | --- | --- | --- |
| 25-120 | 3.2 | Moisture loss | AC |
| 25-120 | 2.8 | Moisture loss | Composite |
| 120-300 | 8.7 | Volatiles | AC |
| 120-300 | 6.4 | Volatiles | Composite |
| 300-520 | 12.4 | Surface groups | AC |
| 300-545 | 9.8 | Surface groups | Composite |
| 520-580 | 68.2 | Carbon oxidation | AC |
| 545-620 | 58.6 | Carbon oxidation | Composite |
| >580 | 7.5 | Residue | AC |
| >620 | 23.4 | Metal oxide residue | Composite |

Table S14. Complete Kinetic Data for DBT Adsorption (Initial concentration: 200 mg/L)

| Time (min) | qₜ (mg/g) ± SD | Removal Efficiency (%) | ln(qₑ-qₜ) | t/qₜ |
| --- | --- | --- | --- | --- |
| 0 | 0 | 0 | 3.74 | - |
| 15 | 18.6 ± 0.8 | 46.5 | 2.89 | 0.81 |
| 30 | 27.4 ± 1.1 | 68.5 | 2.32 | 1.09 |
| 60 | 34.2 ± 1.3 | 85.5 | 1.89 | 1.75 |
| 120 | 38.7 ± 1.2 | 96.8 | 1.29 | 3.10 |
| 180 | 40.8 ± 1.0 | 102.0 | 0.69 | 4.41 |
| 240 | 42.1 ± 0.9 | 105.3 | -0.11 | 5.70 |
| 300 | 42.3 ± 0.8 | 105.8 | -0.69 | 7.09 |
| 360 | 42.3 ± 0.7 | 105.8 | -0.69 | 8.51 |

Table S15. Kinetic Parameters for Different Initial Concentrations

| Initial Conc. (mg/L) | qₑ,exp (mg/g) | k₁ (min⁻¹) | k₂ (g/mg·min) | R₁² | R₂² |
| --- | --- | --- | --- | --- | --- |
| 50 | 12.4 ± 0.6 | 0.019 | 0.0024 | 0.856 | 0.995 |
| 100 | 24.8 ± 0.9 | 0.021 | 0.0021 | 0.875 | 0.997 |
| 200 | 42.3 ± 1.1 | 0.023 | 0.0018 | 0.892 | 0.997 |
| 300 | 51.7 ± 1.4 | 0.025 | 0.0016 | 0.901 | 0.996 |
| 500 | 58.7 ± 1.6 | 0.027 | 0.0014 | 0.915 | 0.995 |

Table S16. Extended Isotherm Analysis

| Model | Parameter | Units | AC | AC-ZnO/Al₂O₃ |
| --- | --- | --- | --- | --- |
| Langmuir | qₘ | mg/g | 35.2 ± 1.1 | 58.7 ± 1.5 |
|  | KL | L/mg | 0.042 ± 0.003 | 0.089 ± 0.005 |
|  | R² | - | 0.988 | 0.995 |
|  | RL (C₀=200) | - | 0.106 | 0.053 |
| Freundlich | KF | (mg/g)(L/mg)^(1/n) | 8.7 ± 0.4 | 15.3 ± 0.6 |
|  | n | - | 2.8 ± 0.1 | 3.2 ± 0.2 |
|  | R² | - | 0.945 | 0.962 |
| Temkin | AT | L/g | 1.42 ± 0.08 | 2.87 ± 0.12 |
|  | bT | J/mol | 156.8 ± 8.2 | 198.4 ± 9.6 |
|  | R² | - | 0.923 | 0.934 |
| D-R | qₘ | mg/g | 32.4 ± 1.2 | 54.8 ± 1.7 |
|  | E | kJ/mol | 8.7 ± 0.4 | 11.2 ± 0.5 |
|  | R² | - | 0.912 | 0.928 |

Table S17. Detailed Thermodynamic Parameters

| Temperature | KL (L/mg) | ln(KL) | ΔG° (kJ/mol) | ΔH° (kJ/mol) | ΔS° (J/mol·K) |
| --- | --- | --- | --- | --- | --- |
| 298 K (25°C) | 0.089 | -2.42 | -10.2 ± 0.3 | -23.7 ± 1.2 | -45.2 ± 2.1 |
| 308 K (35°C) | 0.074 | -2.60 | -9.7 ± 0.4 | -23.7 ± 1.2 | -45.2 ± 2.1 |
| 318 K (45°C) | 0.062 | -2.78 | -9.2 ± 0.3 | -23.7 ± 1.2 | -45.2 ± 2.1 |
| 328 K (55°C) | 0.053 | -2.94 | -8.8 ± 0.5 | -23.7 ± 1.2 | -45.2 ± 2.1 |

Table S18. Effect of pH on Multiple Pollutants Removal

| pH | DBT qₑ (mg/g) | Pb²⁺ Removal (%) | Phenol qₑ (mg/g) | MB qₑ (mg/g) |
| --- | --- | --- | --- | --- |
| 3 | 48.2 ± 1.4 | 78.4 ± 2.1 | 72.3 ± 2.8 | 18.9 ± 0.7 |
| 4 | 52.1 ± 1.6 | 84.7 ± 1.9 | 78.6 ± 2.4 | 20.4 ± 0.8 |
| 5 | 55.8 ± 1.8 | 89.2 ± 1.7 | 82.1 ± 2.1 | 21.8 ± 0.6 |
| 6 | 57.9 ± 1.5 | 93.6 ± 1.4 | 85.8 ± 1.9 | 22.7 ± 0.5 |
| 7 | 58.7 ± 1.3 | 95.2 ± 1.1 | 87.4 ± 1.6 | 23.2 ± 0.4 |
| 8 | 57.4 ± 1.4 | 94.8 ± 1.2 | 86.9 ± 1.8 | 22.9 ± 0.6 |
| 9 | 54.2 ± 1.7 | 92.1 ± 1.5 | 83.7 ± 2.2 | 21.4 ± 0.7 |
| 10 | 49.8 ± 1.9 | 87.3 ± 1.8 | 78.2 ± 2.6 | 19.8 ± 0.9 |
| 11 | 44.6 ± 2.1 | 81.7 ± 2.3 | 71.4 ± 3.1 | 17.6 ± 1.1 |

Table S19. Effect of Common Interfering Ions on DBT Adsorption

| Interfering Ion | Concentration (mg/L) | qₑ without interferent (mg/g) | qₑ with interferent (mg/g) | Interference (%) |
| --- | --- | --- | --- | --- |
| Na⁺ | 100 | 58.7 ± 1.3 | 57.2 ± 1.4 | 2.6 |
| K⁺ | 50 | 58.7 ± 1.3 | 56.8 ± 1.5 | 3.2 |
| Ca²⁺ | 200 | 58.7 ± 1.3 | 54.3 ± 1.7 | 7.5 |
| Mg²⁺ | 100 | 58.7 ± 1.3 | 55.9 ± 1.6 | 4.8 |
| Cl⁻ | 500 | 58.7 ± 1.3 | 57.8 ± 1.2 | 1.5 |
| SO₄²⁻ | 300 | 58.7 ± 1.3 | 56.1 ± 1.8 | 4.4 |
| NO₃⁻ | 100 | 58.7 ± 1.3 | 58.1 ± 1.1 | 1.0 |
| HCO₃⁻ | 150 | 58.7 ± 1.3 | 55.4 ± 1.9 | 5.6 |

Figure S1. Complete nitrogen adsorption-desorption isotherms with pore size distribution analysis

Figure S2. XPS spectra showing surface chemical states

Figure S3. Complete kinetic profiles for all pollutants at different temperatures

Figure S4. 3D response surface plots for optimization studies

Figure S5. Regeneration efficiency over extended cycles (10 cycles)

Figure S6. Pilot-scale column breakthrough curves

Figure S7. Economic feasibility analysis charts