Supplementary Material

Modification of natural pigskin collagen via cryogrinding: a focused study on its physiochemical properties

Yuling Xu et al.

DOI 10.1515/polyeng-2022-0269

Supplementary Table S1: Collagen purity and extraction rates.

| Sample | Control group (%) | G3 (%) | G5 (%) | G10 (%) | G20 (%) |
| --- | --- | --- | --- | --- | --- |
| Purity | 98.2±1.0 | 99.8±0.3 | 95.4±1.5 | 99.6±0.6 | 99.5±0.8 |
| Extraction rate | 22±2.0 | 32±1.0 | 35±2.0 | 37±1.0 | 40±2.0 |

Supplementary Figure S1: DSC curves of the ground collagens.

Thermostability test method

Collagen samples (10 mg) were transferred into 400 μL of pre-cooled 0.1 M acetic acid and dissolved at a low temperature (2–10oC) until they became semi-transparent gels. DSC (Q2000, TA Instruments, USA) was harnessed to discriminate the thermal stability of samples with an empty aluminum box being the blank. The heating rate was 5oC/min with a nitrogen flow rate of 20 mL/min within 20–60oC.

Thermostability test analyses

Based on the DSC curves of samples depicted in Supplementary Figure S1, it is clear that there is no significant difference among samples regarding the thermal denaturation temperature; that is to say, grinding treatment does not change the thermal stability of collagen.