Supplementary material for

Sorption of cobalt from aqueous solution containing EDTA under UV-C irradiation by antimony oxide

This file contains two equations, one figure and one table

Equations:

The propagation of uncertainty is calculated by Equation (S1):

∆f= ∆fx1,x2,…,xn,∆x1,∆x2,…,∆xn=i=1 n(∂f∂xi∆xi)2 		(S1)

where ∆f is the estimated total deviation of f derived from the partial derivate of f with respect to each of the variables x1, x2, …, xn.

E.g. the estimated total deviation of KD is calculated by Equation (S2):

∆KD= ∂KD∂A0∆A02+ ∂KD∂Aeq∆Aeq2+ ∂KD∂V∆V2+ ∂KD∂m∆m2= 1Aeq∆A0Vm2+ -A0Aeq2∆AeqVm2+A0Aeq-1∆Vm2+A0Aeq-1-Vm2∆m2   	(S2)

Figure S1. FESEM (field emission scanning electron microscope, Hitachi S-4800) picture of the particle size distribution of the synthesized antimony oxide.

Table S1. The intensities of the reference material, Sb6O13, and the synthesized antimony oxide as derived from the XRD diffractograms.

|  |  |  | Reference |  |  | Measured |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| h | k | l | d [Å] | 2Theta [deg] | I [%] | d [Å] | 2Theta [deg] | I [%] |
| 1 | 1 | 1 | 5.949 | 14.880 | 25 | 5.906 | 15.0 | 83 |
| 3 | 1 | 1 | 3.108 | 28.700 | 20 | 3.113 | 28.678 | 75 |
| 2 | 2 | 2 | 2.976 | 30.002 | 100 | 2.973 | 30.056 | 100 |
| 4 | 0 | 0 | 2.577 | 34.785 | 30 | 2.596 | 34.545 | 12 |
| 3 | 3 | 1 | 2.365 | 38.017 | 4 | 2.369 | 37.974 | 9 |
| 5 | 1 | 1 | 1.983 | 45.709 | 6 | 1.978 | 45.882 | 14 |
| 4 | 4 | 0 | 1.821 | 50.041 | 25 | 1.818 | 50.187 | 28 |
| 5 | 3 | 1 | 1.741 | 52.501 | 8 | 1.738 | 52.670 | 19 |
| 6 | 2 | 2 | 1.553 | 59.451 | 30 | 1.553 | 59.515 | 20 |
| 4 | 4 | 4 | 1.487 | 62.371 | 9 | 1.486 | 62.521 | 7 |
| 7 | 1 | 1 | 1.443 | 64.518 | 8 | 1.436 | 64.934 | 8 |
| 7 | 3 | 1 | 1.341 | 70.082 | 6 | 1.343 | 69.979 | 7 |

Standard X-ray Diffraction Powder Patterns, National Bureau of Standards (U.S.) Monogr. 25, 16 (1979) pp. 14.