Supplementary Information

Targeted synthesis of carbon-supported titanate nanofibers as host structure for nuclear waste immobilization
Lei Li a, Ran Ma a, Xuewei Liu a Tao Wen a,*, Bo Wu a, Mingtai Sunb, Zheng Jiang,a Suhua Wang a,b, Xiangke Wang a, *
aMOE Key Laboratory of Resources and Environmental Systems Optimization, College of Environmental Science and Engineering, North China Electric Power University, Beijing 102206, P.R. China
bGuangdong Provincial Key Laboratory of Petrochemical Pollution Process and Control, School of Environmental Science and Engineering, Guangdong University of Petrochemical Technology, Maoming, Guangdong 525000, P.R. China
*Corresponding authors: twen@ncepu.edu.cn (T. Wen), xkwang@ncepu.edu.cn (X. Wang). Tel (Fax): 86-10-61772890.
[image: image1.emf]01 2 3 4 5 6 7

C@TNFs 

Intensity (a.u.)

Ti

Ti

Na

Ti

O

 

 

Energy (KeV)

C

a)

0 1 2 3 4 5 6 7

C@TNFs(H) 

Intensity (a.u.)

Energy (KeV)

 

 

 

Ti

Ti

O

Ti

Na

C

b)


Figure S1. EDS spectra of (a) C@TNFs and (b) C@TNFs(H).
[image: image2.emf]10 100

0.00

0.01

0.02

0.03

0.04

0.05

2

5

Relative Diameter 

(

nm

)

dV/dw Pore Volume 

(

cm

3

 g

-1

 nm

-1

)

 

 

 

C@TNFs 

 

C@TNFs(H) 

0.0 0.2 0.4 0.6 0.8 1.0

0

40

80

120

160

61 m

2

 g

-1

 

C@TNFs 

 

C@TNFs(H) 

Quantity adsorbed 

(

cm

3

 g

-1

)

Relative pressure 

(

P/P

0

)

   

 

 

195 m

2

 g

-1

a)

b)


Figure S2. (a) N2 adsorption-desorption isotherms and the corresponding (b) pore size distributions of C@TNFs and C@TNFs(H).

[image: image3.emf]100 200 300 400 500 600 700 800

65

70

75

80

85

90

95

100

Weight loss (%)

Temperature (

o

C)

 

C@TNFs

 C@TNFs(H)

 

 

 

 


Figure S3. TGA curves of C@TNFs and C@TNFs(H).
[image: image4.emf]0 50 100 150 200 250 300 350 400

0

20

40

60 80 100  U(VI)

 Ba(II)

 Sr(II)

Time (min)

   

   

Ion-exchange (%) a) 0 50 100 150 200 250 300 350 400

0

200

400

600

800

1000

1200

 U(VI)

 Ba(II)

 Sr(II)

t/q

t

 

(

min g mmol

-1

)

Time (min)

 

 

 

 

c)

0 50 100 150 200 250 300 350 400

0

20

40

60 80 100 Ion-exchange (%)  U(VI)

 Ba(II)

 Sr(II)

Time (min)

   

   

b) 0 50 100 150 200 250 300 350 400

0

200

400

600

800

1000

1200

 U(VI)

 Ba(II)

 Sr(II)

Time (min)

t/q

t

 

(

min g mmol

-1

)

 

 

 

 

d)


Figure S4. Adsorption kinetic curves of U(VI), Ba(II) and Sr(II) on (a) C@TNFs and (b) C@TNFs(H). The linear simulations of (c) C@TNFs and (d) C@TNFs(H) using pseudo-second-order kinetic model. (C0(U(VI)) = 10.0 ppm, m/V = 0.1 g L-1, pH = 6.0 ± 0.1, and T = 298 K)
[image: image5.emf]1 2 3 4 5 6 7 8 9 10 11 12

0

20

40

60

80

100

 

TNCSs

 TNCSs(H)

pH

Ion-exchange (%)

 

 

 

 

1 2 3 4 5 6 7 8 9 10 11 12

10

3

10

4

10

5

 

K

d

U

 

(

mL

 

g

-1

)

 

 

 

TNCSs

 TNCSs(H)

pH

a)

b)

0 100 200 300 400 500

10

3

10

4

10

5

Ca(II)/U(VI) molar ratio

K

d

U

 

(

mL

 g

-1

)

   

 

 

 

TNCSs

 TNCSs(H)

c)

0 100 200 300 400 500

0

20

40

60

80

100

120

Ion-exchange (%)

 

 

 

 

 

TNCSs

 TNCSs(H)

Ca(II)/U(VI) molar ratio

d)


Figure S5. (a) The values of the distribution coefficient KdU and (b) the ion-exchange percentage at various initial pH values of 2.0-11.0 (C0(U(VI)) = 10.0 ppm, m/V = 0.1 g L-1, and T = 298 K). (c) The values of the distribution coefficient KdU and (d) the ion-exchange percentage at various Ca(II):U(VI) molar ratios of 10-500. (C0(U(VI)) = 10.0 ppm, m/V = 0.1 g L-1, pH = 6.0 ± 0.1, and T = 298 K)
[image: image6.emf]a)b) 800 795 790 785 780 775 770

Ba 3d

C@TNFs(H)

 

  Ba 3d

5/2

Ba 3d

3/2

780.1 eV

795.4 eV

Intensity (a.u.)

Binding Energy (eV)

C@TNFs

 

 

395390 385 380 375

Binding Energy (eV)

Intensity (a.u.)

U 4f

C@TNFs(H)

 

  381.8 eV

392.8 eV

U 4f

5/2

U 4f

7/2

C@TNFs

 

 

140 138 136 134 132 130 128 126

Sr 3d

5/2

Sr 3d

3/2

C@TNFs(H)

 

  133.5 eV

135.3 eV

Sr 3d

Intensity (a.u.)

Binding Energy (eV)

C@TNFs

 

 

c)


Figure S6. High-resolution XPS spectra of (a) U 4f, (b) Ba 3d and (c) Sr 3d.
