Electronic Supporting information

## Separation of ReO4-/TcO4- from simulated radioactive waste liquid by a novel series of anion exchange resins

## Yiwei Huanga,c, Xinlong Chena, Yinglin Shena*, Xiaomin Lia, Xupeng Zhia, Peng Liua, Meiying Liua, Bin Liu*a,b

## a School of Nuclear Science and Technology, Lanzhou university, Lanzhou 730000, China

## b School of Stomatology, Lanzhou University, Lanzhou 730000, China

## c Department Nuclear Medicine,Wuhan University, Zhongnan Hospital, Wuhan 430071, China

#### Preparation of MAGD-1 anion exchange resin

MIMDIDOA ionic liquid was synthesized with reference to previous literature. 1.2 g of 60-80 mesh diatomaceous earth was dried at 65°C for 12 h to remove water and volatiles. It was then mixed with 0.8 g of MIMDIDOA ionic liquid in a 50 mL centrifuge tube, dissolved in 10 mL of methanol and stirred at 25°C for 18 hours. The solvent was removed by distillation in vacuum and dried at 65°C to yield MAGD-1 anion exchange resin as shown in Scheme 2.

#### Preparation of MAPE-1 anion exchange resin

1.2 g of 200 mesh dried AmberchromCG71resin together with 0.8 g of ionic liquid, 10 mL of methanol were added to a 50 mL centrifuge tube and was shaken for 18 h at 25°C. The solvent was removed by distillation in vacuum and dried at 65°C to obtain MAPE-1 resin as shown in Scheme 2.

#### Preparation of MAPE-2 anion exchange resin

1.2g of dried resin, 0.8 g of ionic liquid, 10 mL of methanol were added to a 50 mL centrifuge tube, respectively, and shaking at 25°C for 18 hours. The solvent was removed by distillation in vacuum and dried at 65°C to obtain MAPE-2 resin as shown in Scheme 2.

#### Preparation of MAPE-3 anion exchange resin

1.2 g of 200-mesh dried AmberchromCG71 resin and 0.8 g of MIMDIDTA ionic liquid were added with 10 mL of methanol in a 50 mL centrifuge tube and shaken for 18 h at 25°C. The solvent was removed by distillation in vacuum and dried at 65°C to obtain MAPE-3 resin as shown in Scheme 2.

Fig. S1 1H-NMR for MIMDIDOA

Fig. S2 (a) 1H NMR for MIMDIDEA; (b) 1H NMR for MIMDIDTA

Fig. S3 (a)Cation electrospray mass spectrometry of MIMDIDEA; (b)Cation electrospray mass spectrometry of MIMDIDTA

Fig. S4 The EDS spectra of MAPE-1 and MAPE-1@ReO4-