Separation and Purification of Zr from A Low-Temperature LiCl-KCl-CsCl Eutectic by the Formation of Dendritic Crystal

Daoqing Ma, Jichen Xu, ZhiXuan Yi, Bin Ma, Ming Fang*, Xiaoli Tan*

*Corresponding author: Ming Fang and Xiaoli Tan, a MOE Key Laboratory of Resources and Environmental System Optimization, College of Environmental Science and Engineering, North China Electric Power University, Beijing, 102206, P. R. China,

E-mail: xltan@ncepu.edu.cn; mfang@ncepu.edu.cn

Daoqing Ma, Jichen Xu, ZhiXuan Yi, and Bin Ma, College of Environmental Science and Engineering, North China Electric Power University, Beijing, 102206, P. R. China

Figure. S1: Open circuit voltammogram at 573K on the W electrode after electrodepositing at -2.0 V vs. Ni/Ni2+ for 300s in LiCl-KCl-CsCl-ZrCl4 (2.012×10-4mol cm-3) melts. Working electrode: W (A= 0.322 cm2).

Figure. S2: Current vs. time plots obtained by PE at -2.0 V for 4 h in LiCl-KCl-CsCl-ZrCl4 (2.012×10-4mol cm-3) molten salt.