Supplementary Figure I: 13C-NMR

Supplementary-Figure S1. 13C-NMR spectrum of structure IV based on BU-DA monomer.

Supplementary-Table S1. 13C-NMR peak

assignments of structure IV.

| Peak | Chemical Shift (ppm) |
| --- | --- |
| a, b | 165.27 |
| c, d | 132.64 |
| e | 126.07 |
| f | 66.45 |
| g | 142.25 |
| h | 26.77 |

Supplementary-Figure S2. 13C-NMR spectrum of structure VII based on BU-DA monomer.

| Peak | Chemical Shift (ppm) |
| --- | --- |
| a, b | 165.53 |
| c, d | 132.68 |
| e | 124.74 |
| f | 66.31 |
| h | 26.53 |

Supplementary-Table S2. 13C-NMR peak

assignments of structure VII.

Supplementary Figure II: 1H-NMR

Supplementary Figure III: TGA/DTG