Study on the influence of papermaking process on the properties of Chinese handmade bamboo paper

Fig.S1. Chinese Handmade Paper Bamboo Curtain Schematic

Fig.S2. ATR-FTIR spectra of paper samples. (a) Renhua paper，(b) Changting paper1，(c) Changting paper2，(d) Panxian paper，(e) Fuyang paper，(f) Liancheng paper.

Fig.S3. XRD spectra of paper samples. (a) Renhua paper，(b) Changting paper1，(c) Changting paper2，(d) Panxian paper，(e) Fuyang paper，(f) Liancheng paper aging.

Fig.S4. Scanning electron microscope of paper samples. (a) Renhua paper，(b) Renhua paper aging for 60 days，(c) Changting paper1，(d) Changting paper1 aging for 60 days，(e) Lianchen paper，(f) Lianchen paper aging for 60 days.

SEM-EDS

Renhua paper

FW: 733 μm, Mode: 15 kV - Image, Detector: BSD

|  | Element Number | Element Symbol | Element Name | Atomic Conc. | Weight Conc. |
| --- | --- | --- | --- | --- | --- |
|  | 6 | C | Carbon | 33.272 | 22.000 |
|  | 8 | O | Oxygen | 52.674 | 46.400 |
|  | 14 | Si | Silicon | 0.453 | 0.700 |
|  | 20 | Ca | Calcium | 12.734 | 28.100 |
|  | 28 | Ni | Nickel | 0.867 | 2.800 |

Changting paper1

FW: 799 μm, Mode: 15 kV - Image, Detector: BSD

|  | Element Number | Element Symbol | Element Name | Atomic Conc. | Weight Conc. |
| --- | --- | --- | --- | --- | --- |
|  | 6 | C | Carbon | 29.431 | 19.000 |
|  | 8 | O | Oxygen | 54.880 | 47.200 |
|  | 20 | Ca | Calcium | 15.689 | 33.800 |

Changting paper2

FW: 799 μm, Mode: 15 kV - Image, Detector: BSD

|  | Element Number | Element Symbol | Element Name | Atomic Conc. | Weight Conc. |
| --- | --- | --- | --- | --- | --- |
|  | 6 | C | Carbon | 27.578 | 16.300 |
|  | 8 | O | Oxygen | 49.911 | 39.300 |
|  | 20 | Ca | Calcium | 22.510 | 44.400 |

Fuyang paper

FW: 799 μm, Mode: 15 kV - Image, Detector: BSD

|  | Element Number | Element Symbol | Element Name | Atomic Conc. | Weight Conc. |
| --- | --- | --- | --- | --- | --- |
|  | 6 | C | Carbon | 29.039 | 19.800 |
|  | 8 | O | Oxygen | 59.447 | 54.000 |
|  | 20 | Ca | Calcium | 11.514 | 26.200 |

Liancheng paper

FW: 799 μm, Mode: 15 kV - Image, Detector: BSD

|  | Element Number | Element Symbol | Element Name | Atomic Conc. | Weight Conc. |
| --- | --- | --- | --- | --- | --- |
|  | 6 | C | Carbon | 27.777 | 18.382 |
|  | 8 | O | Oxygen | 58.698 | 51.748 |
|  | 20 | Ca | Calcium | 13.526 | 29.870 |