Supporting Information

Content

Single crystal X-ray structure determinations	2

Figures of the coordination polyhedra	8

Comparison between monoclinic and orthorhombic structure models	11

Knasibfite at 100 K	11

Knasibfite at 400 K	11

Knasibfite at room temperature	11

K3Na4[GeF6]3[BF4] at 100 K	12

K3Na4[GeF6]3[BF4] at 293 K	12

Powder X-ray diffraction measurements	13

Thermogravimetric investigation and DSC	21

IR spectra	22

Raman spectra	23

# Single crystal X-ray structure determinations

Table S 1. Selected crystallographic data and details of the structure determination of K3Na4[SiF6]3[BF4] at 100 K.

| Formula | K3Na4[SiF6]3[BF4] |
| --- | --- |
| Molar mass / g·mol−1 | 722.34 |
| Space group (No.) | I2 (5) |
| a / Å | 5.5003(6) |
| b / Å | 9.0890(9) |
| c / Å | 17.048(2) |
| β / ° | 90.041(9) |
| V / Å3 | 852.2(2) |
| Z | 2 |
| Pearson symbol | mI66 |
| ρcalc. / g·cm−3 | 2.815 |
| ρmeas. / g·cm−3 (25 °C) | 2.70(2) |
| µ / mm−1 | 1.334 |
| Color | colorless |
| Crystal habitus | block |
| Crystal size / mm3 | 0.27 ∙ 0.32 ∙ 0.27 |
| T / K | 100 |
| λ / Å | 0.71073 (Mo- Kα) |
| No. of reflections | 7890 |
| θ range / ° | 3.892 – 31.659 |
| Range of Miller indices | −8 ≤ h ≤ 8 |
|  | −12 ≤ k ≤ 13 |
|  | −25 ≤ l ≤ 24 |
| Absorption correction | numerical |
| Tmax, Tmin | 0.8896, 0.7896 |
| Rint, Rσ | 0.0198, 0.0268 |
| Completeness of the data set | 0.997 |
| No. of unique reflections | 2730 |
| No. of parameters | 152 |
| No. of restrains | 0 |
| No. of constrains | 0 |
| S (all data) | 1.139 |
| R(F) (I ≥ 2σ(I), all data) | 0.0156, 0.0163 |
| wR(F2) (I ≥ 2σ(I), all data) | 0.0401, 0.0413 |
| Extinction coefficient | - |
| Δρmax, Δρmin / e·Å−3 | 0.278, −0.229 |
| fraction of the second twin domaina | 0.463(2) |

- twofold rotation around the a axis as twin element

Table S 2. Selected crystallographic data and details of the structure determination of K3Na4[SiF6]3[BF4] at 400 K.

| Formula | K3Na4[SiF6]3[BF4] |
| --- | --- |
| Molar mass / g·mol−1 | 722.34 |
| Space group (No.) | Im2m (44) |
| a / Å | 5.546(2) |
| b / Å | 9.261(2) |
| c / Å | 17.184(4) |
| V / Å3 | 882.5(4) |
| Z | 2 |
| Pearson symbol | oI66 |
| ρcalc. / g·cm−3 | 2.718 |
| ρmeas. / g·cm−3 (25 °C) | 2.70(2) |
| µ / mm−1 | 1.288 |
| Color | colorless |
| Crystal habitus | block |
| Crystal size / mm3 | 0.05, 0.08, 0.095 |
| T / K | 400 |
| λ / Å | 0.71073 (Mo- Kα) |
| No. of reflections | 8015 |
| θ range / ° | 3.861– 32.588 |
| Range of Miller indices | −8 ≤ h ≤ 8 |
|  | −14 ≤ k ≤ 14 |
|  | −25 ≤ l ≤ 25 |
| Absorption correction | numerical |
| Tmax, Tmin | 0.8748, 0.8043 |
| Rint, Rσ | 0.0483, 0.0604 |
| Completeness of the data set | 0.997 |
| No. of unique reflections | 1802 |
| No. of parameters | 95 |
| No. of restrains | 0 |
| No. of constrains | 0 |
| S (all data) | 0.926 |
| R(F) (I ≥ 2σ(I), all data) | 0.0296, 0.0566 |
| wR(F2) (I ≥ 2σ(I), all data) | 0.0524, 0.0578 |
| Extinction coefficient | - |
| Δρmax, Δρmin / e·Å−3 | 0.262, −0.364 |
| fraction of the second twin domaina | 0.5 |

- inversion twin

Table S 3. Selected crystallographic data and details of the structure determination of K3Na4[GeF6]3[BF4] at 100 K.

| Formula | K3Na4[GeF6]3[BF4] |
| --- | --- |
| Molar mass / g·mol−1 | 855.84 |
| Space group (No.) | I2 (5) |
| a / Å | 5.6221(6) |
| b / Å | 9.2136(6) |
| c / Å | 17.3411(2) |
| β / ° | 90.544(9) |
| V / Å3 | 898.2(1) |
| Z | 2 |
| Pearson symbol | mI66 |
| ρcalc. / g·cm−3 | 3.164 |
| µ / mm−1 | 5.988 |
| Color | colorless |
| Crystal habitus | block |
| Crystal size / mm3 | 0.4 ∙ 0.44 ∙ 0.38 |
| T / K | 100 |
| λ / Å | 0.71073 (Mo- Kα) |
| No. of reflections | 7889 |
| θ range / ° | 3.799 – 31.443 |
| Range of Miller indices | −8 ≤ h ≤ 8 |
|  | −13 ≤ k ≤ 13 |
|  | −25 ≤ l ≤ 25 |
| Absorption correction | numerical |
| Tmax, Tmin | 0.209, 0.178 |
| Rint, Rσ | 0.0329, 0.0476 |
| Completeness of the data set | 0.997 |
| No. of unique reflections | 2795 |
| No. of parameters | 152 |
| No. of restrains | 0 |
| No. of constrains | 0 |
| S (all data) | 1.160 |
| R(F) (I ≥ 2σ(I), all data) | 0.0261, 0.0278 |
| wR(F2) (I ≥ 2σ(I), all data) | 0.0592, 0.0597 |
| Extinction coefficient | 0.0033(3) |
| Δρmax, Δρmin / e·Å−3 | 0.772, −0.639 |

Table S 4. Selected crystallographic data and details of the structure determination of K3Na4[GeF6]3[BF4] at 293 K.

| Formula | K3Na4[GeF6]3[BF4] |
| --- | --- |
| Molar mass / g·mol−1 | 855.84 |
| Space group (No.) | Im2m (44) |
| a / Å | 5.6781(6) |
| b / Å | 9.2879(9) |
| c / Å | 17.494(2) |
| V / Å3 | 922.6(2) |
| Z | 2 |
| Pearson symbol | oI66 |
| ρcalc. / g·cm−3 | 3.081 |
| µ / mm−1 | 5.830 |
| Color | colorless |
| Crystal habitus | block |
| Crystal size / mm3 | 0.4 ∙ 0.44 ∙ 0.38 |
| T / K | 293 |
| λ / Å | 0.71073 (Mo- Kα) |
| No. of reflections | 16402 |
| θ range / ° | 2.483– 45.093 |
| Range of Miller indices | −10 ≤ h ≤ 10 |
|  | −15 ≤ k ≤ 17 |
|  | −34 ≤ l ≤ 34 |
| Absorption correction | numerical |
| Tmax, Tmin | 0.215, 0.184 |
| Rint, Rσ | 0.0585, 0.0854 |
| Completeness of the data set | 0.974 |
| No. of unique reflections | 3826 |
| No. of parameters | 95 |
| No. of restrains | 0 |
| No. of constrains | 0 |
| S (all data) | 1.017 |
| R(F) (I ≥ 2σ(I), all data) | 0.0369, 0.0508 |
| wR(F2) (I ≥ 2σ(I), all data) | 0.0846, 0.0908 |
| Extinction coefficient | - |
| Δρmax, Δρmin / e·Å−3 | 0.747, −1.293 |

Table S 5.Anisotropic displacement parameters (/Å2) for both modifications of K3Na4[SiF6]3[BF4] and K3Na4[GeF6]3[BF4].

| Atom | U11 | U22 | U33 | U23 | U13 | U12 |
| --- | --- | --- | --- | --- | --- | --- |
| K3Na4[SiF6]3[BF4] at 400 K (orthorhombic, Im2m) |  |  |  |  |  |  |
| B | 0.035(3) | 0.028(4) | 0.023(3) | 0 | 0 | 0 |
| F1 | 0.034(2) | 0.027(2) | 0.066(3) | 0 | 0 | 0 |
| F2 | 0.046(2) | 0.027(2) | 0.085(3) | 0 | 0 | 0 |
| F3 | 0.0359(11) | 0.0634(12) | 0.0397(11) | −0.0062(11) | 0.0193(8) | 0.0026(10) |
| F4 | 0.090(2) | 0.0228(14) | 0.063(2) | −0.0089(15) | 0 | 0 |
| F5 | 0.0619(19) | 0.0240(14) | 0.0472(19) | −0.0074(12) | 0 | 0 |
| F6 | 0.0357(10) | 0.0591(13) | 0.0412(11) | 0.0079(11) | 0.0166(8) | 0.0001(10) |
| F7 | 0.0475(11) | 0.0650(15) | 0.0464(12) | 0.0068(12) | −0.0262(10) | −0.0113(10) |
| F8 | 0.0333(14) | 0.0418(15) | 0.0470(16) | 0 | 0 | 0.0050(11) |
| F9 | 0.066(2) | 0.0476(18) | 0.0414(17) | −0.0186(14) | 0 | 0 |
| K1 | 0.0446(5) | 0.0466(6) | 0.0388(6) | 0.0108(5) | 0 | 0 |
| K2 | 0.0297(6) | 0.0299(7) | 0.0345(7) | 0 | 0 | 0 |
| Na1 | 0.0390(10) | 0.0373(10) | 0.0446(12) | −0.0002(10) | 0 | 0 |
| Na2 | 0.0254(7) | 0.0286(8) | 0.0293(8) | 0.0036(6) | 0 | 0 |
| Si1 | 0.0175(7) | 0.0250(8) | 0.0200(7) | 0 | 0 | 0 |
| Si2 | 0.0184(4) | 0.0229(5) | 0.0218(5) | −0.0031(4) | 0 | 0 |
| K3Na4[SiF6]3[BF4] at 100 K (monoclinic, I121) |  |  |  |  |  |  |
| B | 0.0124(14) | 0.0061(13) | 0.0080(12) | 0 | 0.004(3) | 0 |
| F1 | 0.0094(9) | 0.0094(8) | 0.0162(8) | 0 | −0.0010(18) | 0 |
| F2 | 0.0136(9) | 0.0085(8) | 0.0249(10) | 0 | −0.0019(18) | 0 |
| F3A | 0.0102(8) | 0.0188(11) | 0.0111(9) | 0.0023(9) | −0.0047(7) | -0.0003(8) |
| F3B | 0.0125(8) | 0.0161(11) | 0.0113(10) | 0.0001(9) | 0.0045(7) | 0.0021(8) |
| F4 | 0.0274(11) | 0.0080(6) | 0.0170(6) | −0.0025(5) | −0.0011(9) | −0.0013(10) |
| F5 | 0.0185(9) | 0.0083(6) | 0.0135(6) | −0.0015(4) | −0.0028(9) | 0.0000(9) |
| F6A | 0.0096(9) | 0.0185(12) | 0.0181(11) | −0.0060(9) | −0.0061(8) | 0.0009(8) |
| F6B | 0.0131(9) | 0.0187(12) | 0.0111(9) | 0.0034(8) | 0.0042(7) | −0.0001(8) |
| F7A | 0.0195(10) | 0.0191(13) | 0.0166(11) | −0.0033(8) | 0.0094(8) | -−0.0071(9) |
| F7B | 0.0157(8) | 0.0171(10) | 0.0133(10) | 0.0012(8) | −0.0086(8) | −0.0038(8) |
| F8 | 0.0109(6) | 0.0112(5) | 0.0139(6) | −0.0002(12) | −0.0001(11) | 0.0012(4) |
| F9 | 0.0197(8) | 0.0137(6) | 0.0126(6) | −0.0059(4) | −0.0027(12) | 0.0021(12) |
| K1 | 0.0142(2) | 0.01230(18) | 0.01141(17) | 0.00262(15) | -0.0005(3) | −0.0005(4) |
| K2 | 0.0093(3) | 0.0089(3) | 0.0098(2) | 0 | −0.0004(5) | 0 |
| Na1 | 0.0132(4) | 0.0109(4) | 0.0140(4) | 0.0000(3) | −0.0004(8) | 0.0017(8) |
| Na2 | 0.0083(4) | 0.0080(4) | 0.0087(3) | 0.0005(3) | 0.0008(7) | 0.0004(7) |
| Si1 | 0.0064(3) | 0.0078(3) | 0.0066(3) | 0 | −0.0008(6) | 0 |
| Si2 | 0.0069(3) | 0.0068(2) | 0.0071(2) | −0.00048(16) | 0.0000(4) | 0.0002(4) |
| K3Na4[GeF6]3[BF4] at 293 K (orthorhombic, Im2m) |  |  |  |  |  |  |
| B | 0.026(2) | 0.016(2) | 0.0175(18) | 0 | 0 | 0 |
| F1 | 0.029(2) | 0.0214(19) | 0.046(2) | 0 | 0 | 0 |
| F2 | 0.037(2) | 0.0176(18) | 0.064(3) | 0 | 0 | 0 |
| F3 | 0.0361(10) | 0.0506(14) | 0.0384(10) | −0.0019(11) | 0.0251(9) | 0.0056(12) |
| F4 | 0.089(4) | 0.0211(18) | 0.054(2) | −0.0093(16) | 0 | 0 |
| F5 | 0.057(3) | 0.0134(12) | 0.0345(14) | −0.0067(11) | 0 | 0 |
| F6 | 0.0299(9) | 0.0547(16) | 0.0386(10) | 0.0106(12) | 0.0184(8) | 0.0023(12) |
| F7 | 0.0483(14) | 0.053(2) | 0.0456(12) | 0.0083(12) | −0.0326(11) | −0.0147(14) |
| F8 | 0.0277(12) | 0.0295(16) | 0.0387(13) | 0 | 0 | 0.0072(11) |
| F9 | 0.058(2) | 0.0347(17) | 0.0297(13) | −0.0167(13) | 0 | 0 |
| K1 | 0.0380(5) | 0.0344(6) | 0.0301(4) | 0.0070(4) | 0 | 0 |
| K2 | 0.0242(4) | 0.0224(5) | 0.0255(4) | 0 | 0 | 0 |
| Na1 | 0.0325(9) | 0.0283(10) | 0.0338(9) | 0.0000(8) | 0 | 0 |
| Na2 | 0.0167(5) | 0.0212(7) | 0.0185(5) | 0.0022(5) | 0 | 0 |
| Ge1 | 0.01135(16) | 0.0179(2) | 0.01336(16) | 0 | 0 | 0 |
| Ge2 | 0.01382(12) | 0.01607(14) | 0.01480(11) | −0.00257(11) | 0 | 0 |
| K3Na4[GeF6]3[BF4] at 100 K (monoclinic, I121) |  |  |  |  |  |  |
| B | 0.011(3) | 0.007(3) | 0.010(3) | 0 | 0.000(2) | 0 |
| F1 | 0.011(2) | 0.009(2) | 0.024(2) | 0 | −0.0016(18) | 0 |
| F2 | 0.017(2) | 0.0093(19) | 0.027(2) | 0 | −0.0011(17) | 0 |
| F3A | 0.0177(17) | 0.0213(17) | 0.0251(16) | 0.0051(15) | −0.0126(13) | −0.0013(14) |
| F3B | 0.0200(18) | 0.0231(17) | 0.0166(15) | 0.0022(16) | 0.0098(12) | 0.0041(17) |
| F4 | 0.031(2) | 0.0103(16) | 0.0275(18) | −0.0003(15) | −0.0047(15) | −0.0013(15) |
| F5 | 0.0220(19) | 0.0089(16) | 0.0205(17) | −0.0027(12) | −0.0070(14) | 0.0002(13) |
| F6A | 0.0125(15) | 0.0193(18) | 0.0274(17) | −0.0092(13) | −0.0109(12) | 0.0021(12) |
| F6B | 0.0138(15) | 0.0252(16) | 0.0155(13) | 0.0055(16) | 0.0039(11) | 0.0028(17) |
| F7A | 0.0248(19) | 0.0263(19) | 0.0238(16) | −0.0069(18) | 0.0119(13) | −0.0108(19) |
| F7B | 0.0128(16) | 0.0182(18) | 0.0195(15) | 0.0014(12) | −0.0087(12) | −0.0026(11) |
| F8 | 0.0113(15) | 0.0119(14) | 0.0191(15) | −0.0006(12) | −0.0008(11) | 0.0033(11) |
| F9 | 0.0220(19) | 0.0152(15) | 0.0136(15) | −0.0067(13) | −0.0021(13) | 0.0024(12) |
| K1 | 0.0163(5) | 0.0137(5) | 0.0131(5) | 0.0023(4) | −0.0016(4) | −0.0008(4) |
| K2 | 0.0105(7) | 0.0098(6) | 0.0123(6) | 0 | −0.0011(5) | 0 |
| Na1 | 0.0117(10) | 0.0116(9) | 0.0154(10) | −0.0013(8) | −0.0024(8) | 0.0015(7) |
| Na2 | 0.0105(9) | 0.0096(8) | 0.0101(8) | −0.0006(6) | −0.0014(6) | −0.0005(6) |
| Ge1 | 0.0058(3) | 0.0088(3) | 0.0079(3) | 0 | −0.0007(2) | 0 |
| Ge2 | 0.0073(2) | 0.0076(2) | 0.0084(2) | −0.00052(17) | −0.00092(15) | −0.00004(17) |

# Figures of the coordination polyhedra

Figure S 1. Polyhedra around K1. All atoms are displayed with arbitrary radii, fluorine atoms are yellow, K atom is purple.

Figure S 2. Left: Voronoi-Polyhedra around K2. Right: Polyhedra around K2. All atoms are displayed with arbitrary radii, fluorine atoms are yellow, K atoms is purple. The red fluorine atoms are included in our description of the polyhedra and are not in the previously description.

Figure S 3. Left: Voronoi-Polyhedra around Na1. Right: Coordination-Polyhedra around Na1. All atoms are displayed with arbitrary radii, fluorine atoms are yellow, Na atom is green. The red fluorine atoms are included in our description of the polyhedra and are not in the previously description.

Figure S 4.Octaheral-like coordination around Na2. All atoms are displayed with arbitrary radii, fluorine atoms are yellow, Na atom is green.

Figure S 5. Connection from the [BF4]−-polyhedron to the alkali metal cations. All atoms are displayed with arbitrary radii. B atom is brown, Na atoms are green, K atoms are purple and fluorine atoms are yellow.

Figure S 6. Connection from the [SiF6]2−-polyhedra to the alkali metal cations (left (Si1) and right (Si2)). All atoms are displayed with arbitrary radii. Si atoms are grey, Na atoms are green, K atoms are purple and fluorine atoms are yellow.

# Comparison between monoclinic and orthorhombic structure models

To allow for a discrimination between the monoclinic and the orthorhombic crystal structures, refinement results for both crystal systems are given here.

## Knasibfite at 100 K

- As mentioned in the manuscript, Knasibfite crystallizes in the monoclinic modification at 100 K. A refinement in the orthorhombic crystal system, space group Im2m, leads to the R-values which are shown in Table S 6. The refinement in the monoclinic crystal system, space group I2, using a twofold rotation around the a axis as twin element, leads to much smaller R-values (also listed in Table S 6), and thus to a much better structure model in space group I2.

Table S 6. Some selected details of the structure refinement from Knasibfite at 100 K in space group Im2m and I2.

|  | Im2m | I2 |
| --- | --- | --- |
| S (all data) | 1.345 | 1.139 |
| R(F) (I ≥ 2σ(I), all data) | 0.0382, 0.0386 | 0.0156, 0.0163 |
| wR(F2) (I ≥ 2σ(I), all data) | 0.0958, 0.0959 | 0.0401, 0.0413 |

## Knasibfite at 400 K

As mentioned in the manuscript, Knasibfite crystallizes at 400 K in the orthorhombic crystal system, space group Im2m, as an inversion twin (BASF 0.47(7)). If a refinement is carried out in the monoclinic crystal system (β = 90°), space group I2, using a twofold rotation around the a axis as twin element, the R-values as shown in Table S 7 and a BASF of 0.4(1) are obtained. Based on the R-values alone, no clear discrimination may be possible. However, a comparison of the standard uncertainties of the equivalent isotropic displacement parameters of the atoms, especially of those atoms that are split into two positions in the monoclinic crystal structure, shows those in the orthorhombic crystal structure to be much smaller (an example is shown in Table S 7). Therefore, describing the crystal structure in the orthorhombic crystal system is the most reasonable assumption.

Table S 7. Some selected details of the refinement from Knasibfite at 400 K in space group Im2m and I2.

|  | Im2m | I2 |
| --- | --- | --- |
| S (all data) | 0.926 | 0.893 |
| R(F) (I ≥ 2σ(I), all data) | 0.0296, 0.0566 | 0.0332, 0.0752 |
| wR(F2) (I ≥ 2σ(I), all data) | 0.0524, 0.0578 | 0.0480, 0.0547 |
| UIso/Å² | F3: 0.0464(5) | F3A: 0.058(3), F3B: 0.036(2) |
|  | F6: 0.0453(5) | F6A: 0.047(2), F6B: 0.043(2) |
|  | F7: 0.0530(6) | F7A: 0.058(3), F7B: 0.047(2) |

## Knasibfite at room temperature

As mentioned in the manuscript, Knasibfite crystallizes at 293 K in the orthorhombic crystal system, space group Im2m. If a refinement is carried out in the monoclinic crystal system (β = 90°), space group I2, using a twofold rotation around the a axis as twin element, R-values (Table S 8) are obtained that allow for no clear distinction as was the case for the crystal structure determination at 400 K. As above, a comparison of the standard uncertainties of the equivalent isotropic displacement parameters of the atoms, especially of those atoms that are split into two positions in the monoclinic crystal structure (compare Table S 8), shows those in the orthorhombic crystal structure to be much smaller. Therefore, describing the crystal structure in the orthorhombic crystal system is the most reasonable assumption.

Table S 8. Some selected details of the refinement from K3Na4[SiF6]3[BF4] at 293 K in space group Im2m and I2.

|  | Im2m | I2 |
| --- | --- | --- |
| S (all data) | 1.016 | 0.980 |
| R(F) (I ≥ 2σ(I), all data) | 0.0193, 0.0215 | 0.0223, 0.0257 |
| wR(F2) (I ≥ 2σ(I), all data) | 0.0452, 0.0456 | 0.0505, 0.0513 |
| UIso/Å² | F3: 0.0333(3) | F3A: 0.034(2), F3B: 0.032(2) |
|  | F6: 0.0333(3) | F6A: 0.038(2), F6B: 0.029(1) |
|  | F7: 0.0397(3) | F7A: 0.037(2), F7B: 0.047(2) |

## K3Na4[GeF6]3[BF4] at 100 K

K3Na4[GeF6]3[BF4] crystallizes at 100 K in the monoclinic crystal system, space group I2. A refinement in the orthorhombic crystal system, space group Im2m leads to much higher R-values, which can be seen in Table S 9. So, the structure model in space group I2 is clearly superior.

Table S 9. Some selected details of the refinement from K3Na4[GeF6]3[BF4] at 100 K in space group Im2m and I2.

|  | Im2m | I2 |
| --- | --- | --- |
| S (all data) | 1.178 | 1.160 |
| R(F) (I ≥ 2σ(I), all data) | 0.0788, 0.0796 | 0.0261, 0.0278 |
| wR(F2) (I ≥ 2σ(I), all data) | 0.1728, 0.1733 | 0.0592, 0.0597 |

## K3Na4[GeF6]3[BF4] at 293 K

K3Na4[GeF6]3[BF4] crystallizes at room temperature in the orthorhombic space group Im2m Refinement was carried out as an inversion twin (BASF 0.02(1)). In the monoclinic crystal system, space group I2, a refinement as a fourfold twin (two-fold rotation around the a axis plus inversion) shows only the presence of a mirror plane parallel to the b axis as the twin element (BASF 0.47(2)). The refinement results in the R-values given in Table S 10. The two structure models are extremely similar, as the refinement in the monoclinic system yields a structure model that is essentially identical to the orthorhombic case, so that no significant discrimination is possible. As is common sense in crystallography, the higher symmetry is chosen. Also, the standard uncertainties of the isotropic equivalent displacement parameters of the atoms that are split upon transition to I2 are smaller in Im2m.

Table S 10. Some selected details of the refinement from K3Na4[GeF6]3[BF4] at 293 K in space group Im2m and I2.

|  | Im2m | I2 |
| --- | --- | --- |
| S (all data) | 1.017 | 0.984 |
| R(F) (I ≥ 2σ(I), all data) | 0.0369, 0.0508 | 0.397, 0.595 |
| wR(F2) (I ≥ 2σ(I), all data) | 0.0846, 0.0908 | 0.0916, 0.1077 |
| UIso/Å² | F3: 0.0417(6) | F3A: 0.045(2), F3B: 0.038(2) |
|  | F6: 0.0411(6) | F6A: 0.039(2), F6B: 0.044(2) |
|  | F7: 0.0489(9) | F7A: 0.047(2), F7B: 0.051(3) |

# Powder X-ray diffraction measurements

Figure S 7. Powder X-ray diffraction pattern of Knasibfite synthesized at room temperature. Experimental data (dots), Rietveld refinement (red), and difference profile (bottom, black). The calculated reflection positions are shown as black ticks: K[BF4] (first row), Na2SiF6 (second row) and Knasibfite (third row).

Table S 11. Selected crystallographic data and details of the Rietveld refinement of K3Na4[SiF6]3[BF4] which was synthesized at room temperature.

| Formula | K3Na4[SiF6]3[BF4] |
| --- | --- |
| Molar mass / g·mol−1 | 722.34 |
| Space group (No.) | Im2m (44) |
| a / Å | 5.5337(3) |
| b / Å | 9.1952(4) |
| c / Å | 17.1502(8) |
| V / Å3 | 872.66(7) |
| Z | 2 |
| Pearson symbol | oI66 |
| ρcalc. / g·cm−3 | 2.7488 |
| Color of the powder | colorless |
| T / K | 293 |
| λ / Å | 1.54060 (Cu-Kα1) |
| 2θmin, 2θmax, 2θstep / ° | 5.000, 82.790, 0.015 |
| No. of data points | 5187 |
| No. of parameters | 79 |
| No. of restrains | 6 |
| No. of constrains | 1 |
| Peak shape function | Gaussian |
| Background | manual |
| S | 1.67 |
| Rp, Rwp * | 31.45, 28.74 |
| Rp, Rwp | 8.95, 12.05 |
| RB(I) | 13.01 |
| Δρmax, Δρmin / e·Å−3 | 0.76, −0.86 |
| Other phases | Na2[SiF6] (22(1) %), K[BF4] (6(1) %) |

* Background-corrected R-factors

Figure S 8. Powder X-ray diffraction pattern of Knasibfite synthesized at 200 °C. Experimental data (dots), Rietveld refinement (red), and difference profile (bottom, black). The calculated reflection positions are shown as black ticks: Na2[SiF6] (first row) and Knasibfite (second row).

Table S 12. Selected crystallographic data and details of the Rietveld refinement of K3Na4[SiF6]3[BF4] which was synthesized at 200 °C.

| Formula | K3Na4[SiF6]3[BF4] |
| --- | --- |
| Molar mass / g·mol−1 | 722.34 |
| Space group (No.) | Im2m (44) |
| a / Å | 5.5305(5) |
| b / Å | 9.1896(9) |
| c / Å | 17.138(2) |
| V / Å3 | 871.0(1) |
| Z | 2 |
| Pearson symbol | oI66 |
| ρcalc. / g·cm−3 | 2.754 |
| Color of the powder | colorless |
| T / K | 293 |
| λ / Å | 1.54060 (Cu-Kα1) |
| 2θmin, 2θmax, 2θstep / ° | 6.000, 75.78, 0.015 |
| No. of data points | 4653 |
| No. of parameters | 76 |
| No. of restrains | 1 |
| No. of constrains | 1 |
| Peak shape function | Pseudo-Voigt |
| Background | 15 Legendre polynoms |
| S | 0.98 |
| Rp, Rwp * | 22.39, 17.70 |
| Rp, Rwp | 4.36, 6.03 |
| RB(I) | 10.30 |
| Δρmax, Δρmin / e·Å−3 | 0.49, −0.41 |
| Other phase | Na2[SiF6] (3.6(6) %)) |

* Background-corrected R-factors

Figure S 9. Powder X-ray diffraction pattern of K3Na4[GeF6]3[BF4] synthesized at room temperature. Experimental data (dots), Rietveld refinement (red), and difference profile (bottom, black). The calculated reflection positions are shown as black ticks: K2[GeF6] (first row) and K3Na4[GeF6]3[BF4] (second row).

Table S 13. Selected crystallographic data and details of the Rietveld refinement of K3Na4[GeF6]3[BF4] which was synthesized at room temperature.

| Formula | K3Na4[GeF6]3[BF4] |
| --- | --- |
| Molar mass / g·mol−1 | 855.8 |
| Space group (No.) | Im2m (44) |
| a / Å | 5.6675(8) |
| b / Å | 9.272(1) |
| c / Å | 17.461(2) |
| V / Å3 | 917.6(2) |
| Z | 2 |
| Pearson symbol | oI66 |
| ρcalc. / g·cm−3 | 3.0974 |
| Color of the powder | colorless |
| T / K | 293 |
| λ / Å | 1.54060 (Cu-Kα1) |
| 2θmin, 2θmax, 2θstep / ° | 6.000, 76.485, 0.015 |
| No. of data points | 4700 |
| No. of parameters | 64 |
| No. of restrains | 0 |
| No. of constrains | 1 |
| Peak shape function | Pseudo-Voigt |
| Background | manual |
| S | 1.69 |
| Rp, Rwp * | 23.75, 22.29 |
| Rp, Rwp | 5.78, 8.82 |
| RB(I) | 11.94 |
| Δρmax, Δρmin / e·Å−3 | 0.79, −1.1 |
| Other phase | K2[GeF6] (51(1) %) |

* Background-corrected R-factors

Figure S 10. Powder X-ray diffraction pattern of K3Na4[GeF6]3[BF4] synthesized at 200 °C. Experimental data (dots), Rietveld refinement (red), and difference profile (bottom, black). The calculated reflection positions are shown as black ticks: K[BF4] (first row), Na2[GeF6] (second row) and K3Na4[GeF6]3[BF4] (third row).

Table S 14. Selected crystallographic data and details of the Rietveld refinement of K3Na4[GeF6]3[BF4] which was synthesized at 200 °C.

| Formula | K3Na4[GeF6]3[BF4] |
| --- | --- |
| Molar mass / g·mol−1 | 855.8 |
| Space group (No.) | Im2m (44) |
| a / Å | 5.6781(6) |
| b / Å | 9.2879(9) |
| c / Å | 17.494(2) |
| V / Å3 | 922.6 (2) |
| Z | 2 |
| Pearson symbol | oI66 |
| ρcalc. / g·cm−3 | 3.0806 |
| Color of the powder | colorless |
| T / K | 293 |
| λ / Å | 1.54060 (Cu-Kα1) |
| 2θmin, 2θmax, 2θstep / ° | 3.000, 83.985, 0.015 |
| No. of data points | 5400 |
| No. of parameters | 83 |
| No. of restrains | 12 |
| No. of constrains | 1 |
| Peak shape function | Gaussian |
| Background | manual |
| S | 1.35 |
| Rp, Rwp * | 37.44, 35.21 |
| Rp, Rwp | 10.72, 14.60 |
| RB(I) | 20.89 |
| Δρmax, Δρmin / e·Å−3 | 1.44, −1.37 |
| Other phase | Na2[GeF6] (48(2) %), K[BF4] (15(2) %) |

* Background-corrected R-factors

# Thermogravimetric investigation and DSC

Knasibfite was thermally decomposed in a stream of nitrogen with heating rates of 1, 5 and 10 K/min. The decomposition starts at 285 °C and the results of the measurement with 5 K/min is shown in Figure S 11.

Figure S 11. Thermal decomposition of Knasibfite in a stream of nitrogen at a heating rate of 5 K/min. The black graph shows the mass loss, the red one the DSC signal.

# IR spectra

Figure S 12. Infrared spectrum of Knasibfite measured on a Bruker Alpha Platinum FT-IR spectrometer using the ATR Diamond module. No experimentally observed IR bands below 400 cm–1 are given due to the limitation of the instrument. The noise between 1900 and 2300 cm–1 is due to the absorption of the diamond.

Figure S 13. Infrared spectrum of K3Na4[GeF6]3[BF4] measured on a Bruker Alpha Platinum FT-IR spectrometer using the ATR Diamond module. No experimentally observed IR bands below 400 cm–1 are given due to the limitation of the instrument. The noise between 1900 and 2300 cm–1 is due to the absorption of the diamond.

# Raman spectra

Figure S 14. Raman spectrum of K3Na4[SiF6]3[BF4] measured with a Confocal Raman Microscope S+I MonoVista CRS+, using the 532 nm excitation line of an integrated diode laser.

Figure S 15. Raman spectrum of K3Na4[GeF6]3[BF4] measured with a Confocal Raman Microscope S+I MonoVista CRS+, using the 532 nm excitation line of an integrated diode las